DNV EH32 STEEL PLATE

Gangsteel is specialized in supplying DNV high strength steel plate in DNV Grade E32. For more information of Grade E32 steel plate, please check them in following:

| DNV EH32 high Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| DNV EH32 | 0.18 | 0.10-0.50 | 0.9-1.6 | 0.035 | 0.035 | 0.015-0.08 | - |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.20 | 0.40 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| DNV EH32 high general strength property |
| --- |
| Grade |  | Mechanical Property | Charpy V Impact Test |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| DNV EH32 | mm | Min Mpa | Mpa | Min % | -40 | J | J |
|  | t≤50 | 315 | 440-590 | 22% |  | 22 | 31 |
|  | 50＜t≤70 | 315 | 440-590 | 22% |  | 26 | 38 |
|  | 70＜t≤150 | 315 | 440-590 | 22% |  | 31 | 46 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of DNV EH32 |
| --- |
| ABS | GL | LR | BV | CCS | NK | KR | RINA |
| AB/EH32 | GL-E32 | LR/EH32 | BV/EH32 | CCS/E32 | K E32 | R E32 | RI/E32 |