DNV EH36 STEEL PLATE

Gangsteel is specialized in supplying DNV high strength steel plate in DNV Grade E36. For more information of Grade E36 steel plate, please check them in following:

| DNV EH36 high Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| DNV EH36 | 0.18 | 0.10-0.50 | 0.9-1.6 | 0.035 | 0.035 | 0.015-0.08 | - |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.20 | 0.40 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| DNV EH36 high general strength property |
| --- |
| Grade |  | Mechanical Property | Charpy V Impact Test |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| DNV EH36 | mm | Min Mpa | Mpa | Min % | -40 | J | J |
|  | t≤50 | 355 | 490-620 | 21% |  | 24 | 34 |
|  | 50＜t≤70 | 355 | 490-620 | 21% |  | 27 | 41 |
|  | 70＜t≤150 | 355 | 490-620 | 21% |  | 34 | 50 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of DNV EH36 |
| --- |
| ABS | GL | LR | BV | CCS | NK | KR | RINA |
| AB/E36 | GL-E36 | LR/E36 | BV/E36 | CCS/E36 | K E36 | R E36 | RI/E36 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.