DNV GRADE D STEEL PLATE

Gangsteel is specialized in supplying DNV general strength steel plate in DNV Grade D. For more information of Grade D steel plate, please check them in following:

| DNV GRADE D general Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| DNV GRADE D | 0.21 | 0.10-0.35 | 0.60 | 0.035 | 0.035 | 0.015 |  |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| DNV GRADE D general strength property |
| --- |
| Grade |  | Mechanical Property | Charpy V Impact Test |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| DNV GRADE D | mm | Min Mpa | Mpa | Min % | -20 | J | J |
|  | t≤50 | 235 | 400-520 | 22% |  | 20 | 27 |
|  | 50＜t≤70 | 235 | 400-520 | 22% |  | 24 | 34 |
|  | 70＜t≤150 | 235 | 400-520 | 22% |  | 27 | 41 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of DNV GRADE D |
| --- |
| ABS | GL | LR | BV | CCS | NK | KR | RINA |
| AB/D | GL-D | LR/D | BV/D | CCS/D | K D | R D | RI/D |