ABS DQ51 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade DQ51. For more information of Grade DQ51 steel plate, please check them in following:

| ABS DQ51 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS DQ51 | 0.20 | 0.55 | 1.7 | 0.030 | 0.030 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS DQ51 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -20 | J | J |
| ABS DQ51 | 500 | 610-770 | 16 |  | 33 | 50 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS DQ51 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV D500 | GL-D500 | LR/DH50 | BV/D500 | CCS/D500 | K D51 | R D51 | RI/D500 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.