ABS EQ51STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade EQ51. For more information of Grade EQ51 steel plate, please check them in following:

| ABS EQ51 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS EQ51 | 0.20 | 0.55 | 1.7 | 0.030 | 0.030 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS EQ51Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -40 | J | J |
| ABS EQ51 | 500 | 610-770 | 16 |  | 33 | 50 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS EQ51 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV E500 | GL-E500 | LR/EH50 | BV/E500 | CCS/E500 | K E51 | R E51 | RI/E500 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.