ABS EQ63 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade EQ63. For more information of Grade EQ63 steel plate, please check them in following:

| ABS EQ63 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS EQ63 | 0.20 | 0.55 | 1.7 | 0.030 | 0.030 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS EQ63 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -40 | J | J |
| ABS EQ63 | 620 | 720-890 | 15 |  | 41 | 62 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS EQ63 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV E620 | GL- E620 | LR/EH62 | BV/E620 | CCS/E620 | K E63 | R E63 | RI/E620 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.