ABS FQ43 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade FQ43. For more information of Grade FQ43 steel plate, please check them in following:

| ABS FQ43 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| AB/FQ43 | 0.18 | 0.55 | 1.6 | 0.025 | 0.025 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS FQ43 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -20 | J | J |
| AB/FQ43 | 420 | 530-680 | 18 |  | 27 | 41 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS FQ43 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV F420 | GL-F420 | LR/FH42 | BV/F420 | CCS/F420 | K F43 | R F43 | RI/F420 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.