ABS FQ70 STEEL PLATE

Gangsteel is specialized in supplying ABS Extra high strength steel plate in ABS Grade FQ70. For more information of Grade FQ70 steel plate, please check them in following:

| ABS FQ70 Extra high Strength Chemical Composition in Tempering and Quenching |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | N |
| ABS FQ70 | 0.18 | 0.55 | 1.60 | 0.025 | 0.025 | 0.02 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| ABS FQ70 Extra high strength property in tempering and quenching |
| --- |
| Grade | Mechanical Property | Charpy V Impact Test |
|  | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
|  | Min Mpa | Mpa | Min % | -60 | J | J |
| ABS FQ70 | 690 | 770-940 | 14 |  | 41 | 62 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate

| Equivalent steel grade of ABS FQ70 |
| --- |
| DNV | GL | LR | BV | CCS | NK | KR | RINA |
| NV F690 | GL-F690 | LR/FH69 | BV/F690 | CCS/F690 | K F70 | R F70 | RI/F690 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.