DNV FH40 STEEL PLATE

Gangsteel is specialized in supplying DNV high strength steel plate in DNV Grade F40. For more information of Grade F40 steel plate, please check them in following:

| DNV FH40 high Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| DNV FH40 | 0.16 | 0.10-0.50 | 0.9-1.6 | 0.025 | 0.025 | 0.015-0.08 | - |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.20 | 0.80 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| DNV FH40 high general strength property |
| --- |
| Grade |  | Mechanical Property | Charpy V Impact Test |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| DNV FH40 | mm | Min Mpa | Mpa | Min % | -60 | J | J |
|  | t≤50 | 390 | 510-650 | 20% |  | 27 | 41 |
|  | 50＜t≤70 | 390 | 510-650 | 20% |  | 30 | 45 |
|  | 70＜t≤150 | 390 | 510-650 | 20% |  | 37 | 55 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of DNV FH40 |
| --- |
| ABS | GL | LR | BV | CCS | NK | KR | RINA |
| AB/F40 | GL-F40 | LR/F40 | BV/F40 | CCS/F40 | K F40 | R F40 | RI/F40 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.