MR0175 A514GRA,A514GRA Steel,A514GRA HIC,A514GRA NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASTM A514 A514GRA NACE MR0175, MR0103 Boiler or pressure vessel steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

A514GRA,ASTM A514GRA,A514GRA Steel Plate,A514GRA HIC,A514GRA Nace

Tags: A514GRA,ASTM A514GRA,A514GRA Steel Plate,A514GRA steel factory, A514GRA adopt standard, A514GRA Heat treatment, A514GRA Technical delivery condition, A514GRA Chemical, A514GRA Mechanical property, A514GRA Price, A514GRA CEV, A514GRA Impact degree, A514GRA impact energy, A514GRA Supplier,A514GRA Specification, A514GRA properties, Material A514GRA N, A514GRA Material, ASTMA514GRA, A514GRA Steel, A514GRA Yield, A514GRA plate, A514GRA HIC, A514GRA NACE MR0175, A514GRA ISO 15156, A514GRA NACE MR0103, A514GRA SSC

Keyword: A514GRA,ASTM A514GRA,A514GRA Steel,A514GRA HIC,A514GRA NACE

- A514GRA Adopt standard: ASTM A514 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- A514GRA Specification:  Thickness: 1mm to 500mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for A514GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- A514GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | P % | S % | V % | AL % | Cr % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A514GRA | 0.24 | 0.13-0.55 | 0.64-1.46 | 0.035 | 0.035 |  |  | 0.29 |
|  | Cu % | Mo % | Nb % | Ni % | Ti % |  |  |  |
|  | 0.38 | 0.09 |  | 0.28 |  |  |  |  |

- A514GRA Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| A514GRA | 5-65 | 345 Mpa | 485-620 Mpa | 22% |  |  |
|  | 65-100 | 310 Mpa | 450-585 Mpa | 18% |  |  |
|  | 100-150 |  |  |  |  |  |

Normally ASTM A514GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

ASTM A514GRA steel plates shall be ASTM A514GrA plate is High-Yield-Strength, Quenched and Tempered Alloy Steel

Plate, Suitable for Welding. ASTM A514GrA plates shall be Quenched and Tempered.

- A514GRA Delivery Time Or Lead Time: 15-30days

- A514GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for A514GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASTMA514 A514GRA NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

A514GRA,ASTM A514GRA,A514GRA Steel Plate,A514GRA HIC,A514GRA Nace

Tags: A514GRA,ASTM A514GRA,A514GRA Steel Plate,A514GRA steel factory, A514GRA adopt standard, A514GRA Heat treatment, A514GRA Technical delivery condition, A514GRA Chemical, A514GRA Mechanical property, A514GRA Price, A514GRA CEV, A514GRA Impact degree, A514GRA impact energy, A514GRA Supplier,A514GRA Specification, A514GRA properties, Material A514GRA N, A514GRA Material, ASTMA514GRA, A514GRA Steel, A514GRA Yield, A514GRA plate, A514GRA HIC, A514GRA NACE MR0175, A514GRA ISO 15156, A514GRA NACE MR0103, A514GRA SSC