A516 GRADE 55 MR0175,A516 GRADE 55 Steel,A516 GRADE 55 HIC,A516 GRADE 55 NACE

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASTM A516 A516 GRADE 55 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

A516 GRADE 55,ASTM A516 GRADE 55,A516 GRADE 55 Steel Plate,A516 GRADE 55 HIC,A516 GRADE 55 Nace

Tags: A516 GRADE 55,ASTM A516 GRADE 55,A516 GRADE 55 Steel Plate,A516 GRADE 55 steel factory, A516 GRADE 55 adopt standard, A516 GRADE 55 Heat treatment, A516 GRADE 55 Technical delivery condition, A516 GRADE 55 Chemical, A516 GRADE 55 Mechanical property, A516 GRADE 55 Price, A516 GRADE 55 CEV, A516 GRADE 55 Impact degree, A516 GRADE 55 impact energy, A516 GRADE 55 Supplier,A516 GRADE 55 Specification, A516 GRADE 55 properties, Material A516 GRADE 55 N, A516 GRADE 55 Material, ASTM A516 GRADE 55, A516 GRADE 55 Steel, A516 GRADE 55 Yield, A516 GRADE 55 plate, A516 GRADE 55 HIC, A516 GRADE 55 NACE MR0175, A516 GRADE 55 ISO 15156, A516 GRADE 55 NACE MR0103, A516 GRADE 55 SSC

Keyword: A516 GRADE 55,ASTM A516 GRADE 55,A516 GRADE 55 Steel,A516 GRADE 55 HIC,A516 GRADE 55 NACE

- A516 GRADE 55 Adopt standard: ASTM SA516 Standard Specification for High-Strength Low-Alloy Columbium-Vanadium Structural Steel

- A516 GRADE 55 Specification:  Thickness: 1mm to 100mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for A516 GRADE 55: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- A516 GRADE 55 Chemical composition % of the Product analysis of grade

| Grade | SA516Gr.55 Chemical Composition, Max (%) |
| --- | --- |
|  | C | Si | Mn | P | S |
| A516 GRADE 55 | 0.18-0.26 | 0.13-0.45 | 0.55-1.30 | 0.035 | 0.035 |

- A516 GRADE 55 Mechanical Property

| Grade | SA516Gr.55 Mechanical Property |
| --- | --- |
|  | Thickness | Yield | Tensile | Elongation |
| A516 GRADE 55 | mm | Min Mpa | Mpa | Min % |
|  | 5-50 | 205 | 380-515 | 27% |
|  | 50-200 | 205 | 380-515 | 23% |

- A516 GRADE 55 Delivery Time Or Lead Time: 15-30days

- A516 GRADE 55 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for A516 GRADE 55, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting ASTM A516 A516 GRADE 55 NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

A516 GRADE 55,ASTM A516 GRADE 55,A516 GRADE 55 Steel Plate,A516 GRADE 55 HIC,A516 GRADE 55 Nace

Tags: A516 GRADE 55,ASTM A516 GRADE 55,A516 GRADE 55 Steel Plate,A516 GRADE 55 steel factory, A516 GRADE 55 adopt standard, A516 GRADE 55 Heat treatment, A516 GRADE 55 Technical delivery condition, A516 GRADE 55 Chemical, A516 GRADE 55 Mechanical property, A516 GRADE 55 Price, A516 GRADE 55 CEV, A516 GRADE 55 Impact degree, A516 GRADE 55 impact energy, A516 GRADE 55 Supplier,A516 GRADE 55 Specification, A516 GRADE 55 properties, Material A516 GRADE 55 N, A516 GRADE 55 Material, ASTM A516 GRADE 55, A516 GRADE 55 Steel, A516 GRADE 55 Yield, A516 GRADE 55 plate, A516 GRADE 55 HIC, A516 GRADE 55 NACE MR0175, A516 GRADE 55 ISO 15156, A516 GRADE 55 NACE MR0103, A516 GRADE 55 SSC