A283GRD,A283GRD Steel Plate,A283GRD Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A283/A283M A283GRD NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A283GRD,A283/A283M A283GRD,A283GRD Steel Plate,A283GRD HIC,A283GRD Nace

Tags: A283GRD,A283/A283M A283GRD,A283GRD Steel Plate,A283GRD steel factory, A283GRD adopt standard, A283GRD Heat treatment, A283GRD Technical delivery condition, A283GRD Chemical, A283GRD Mechanical property, A283GRD Price, A283GRD CEV, A283GRD Impact degree, A283GRD impact energy, A283GRD Supplier,A283GRD Specification, A283GRD properties, Material A283GRD N, A283GRD Material, A283/A283M, A283GRD Steel, A283GRD Yield, A283GRD plate, A283GRD HIC, A283GRD NACE MR0175, A283GRD ISO 15156, A283GRD NACE MR0103, A283GRD SSC

Keyword: A283GRD,A283GRD Steel Plate,A283GRD Supplier

1.  A283GRD Adopt standard: ASMT A283/A283M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  A283GRD Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A283GRD: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A283GRD Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Cu%(min) | Cu%(<=40mm) | Cu%(>40mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A283GRD | 0.27 | 0.9 | 0.035 | 0.04 | 0.2 | 0.4 | 0.15-0.4 |

5.  A283GRD Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A283GRD | 230 Mpa | 415-550Mpa | <=50MM | 23% |
|  | 230 Mpa | 415-550Mpa | 50-200MM | 20% |

6.  Normally A283/A283M A283GRD plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A283GRD Delivery Time Or Lead Time: 20-35days

8.  A283GRD Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A283GRD, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A283/A283M A283GRD NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A283GRD,A283/A283M A283GRD,A283GRD Steel Plate,A283GRD HIC,A283GRD Nace

Tags: A283GRD,A283/A283M A283GRD,A283GRD Steel Plate,A283GRD steel factory, A283GRD adopt standard, A283GRD Heat treatment, A283GRD Technical delivery condition, A283GRD Chemical, A283GRD Mechanical property, A283GRD Price, A283GRD CEV, A283GRD Impact degree, A283GRD impact energy, A283GRD Supplier,A283GRD Specification, A283GRD properties, Material A283GRD N, A283GRD Material, A283/A283M, A283GRD Steel, A283GRD Yield, A283GRD plate, A283GRD HIC, A283GRD NACE MR0175, A283GRD ISO 15156, A283GRD NACE MR0103, A283GRD SSC