A387-22L,A387-22L Steel Plate,A387-22L Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387-22L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. A387-22L,A387/A387M A387-22L,A387-22L Steel Plate,A387-22L HIC,A387-22L Nace

Tags: A387-22L,A387/A387M A387-22L,A387-22L Steel Plate,A387-22L steel factory, A387-22L adopt standard, A387-22L Heat treatment, A387-22L Technical delivery condition, A387-22L Chemical, A387-22L Mechanical property, A387-22L Price, A387-22L CEV, A387-22L Impact degree, A387-22L impact energy, A387-22L Supplier,A387-22L Specification, A387-22L properties, Material A387-22L N, A387-22L Material, A387/A387M, A387-22L Steel, A387-22L Yield, A387-22L plate, A387-22L HIC, A387-22L NACE MR0175, A387-22L ISO 15156, A387-22L NACE MR0103, A387-22L SSC

Keyword: A387-22L,A387-22L Steel Plate,A387-22L Supplier

1.  A387-22L Adopt standard: ASMT A387/A387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  A387-22L Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A387-22L: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A387-22L Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387-22L | 0.12 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 1.88-2.62 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  A387-22L Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A387-22L | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally A387/A387M A387-22L plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A387-22L Delivery Time Or Lead Time: 20-35days

8.  A387-22L Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A387-22L, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387-22L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A387-22L,A387/A387M A387-22L,A387-22L Steel Plate,A387-22L HIC,A387-22L Nace

Tags: A387-22L,A387/A387M A387-22L,A387-22L Steel Plate,A387-22L steel factory, A387-22L adopt standard, A387-22L Heat treatment, A387-22L Technical delivery condition, A387-22L Chemical, A387-22L Mechanical property, A387-22L Price, A387-22L CEV, A387-22L Impact degree, A387-22L impact energy, A387-22L Supplier,A387-22L Specification, A387-22L properties, Material A387-22L N, A387-22L Material, A387/A387M, A387-22L Steel, A387-22L Yield, A387-22L plate, A387-22L HIC, A387-22L NACE MR0175, A387-22L ISO 15156, A387-22L NACE MR0103, A387-22L SSC