GB/T 19189 07MnNiMoDR, 07MnNiMoDR STEEL PLATE,07MnNiMoDR Boiler steel plate

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 19189 07MnNiMoDR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,Quenched and tempered high strength steel plates for pressure vessels,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

07MnNiMoDR,GB/T 19189 07MnNiMoDR,07MnNiMoDR Steel Plate,07MnNiMoDR HIC,07MnNiMoDR Nace

Tags: 07MnNiMoDR,GB/T 19189 07MnNiMoDR,07MnNiMoDR Steel Plate,07MnNiMoDR steel factory, 07MnNiMoDR adopt standard, 07MnNiMoDR Heat treatment, 07MnNiMoDR Technical delivery condition, 07MnNiMoDR Chemical, 07MnNiMoDR Mechanical property, 07MnNiMoDR Price, 07MnNiMoDR CEV, 07MnNiMoDR Impact degree, 07MnNiMoDR impact energy, 07MnNiMoDR Supplier,07MnNiMoDR Specification, 07MnNiMoDR properties, Material 07MnNiMoDR N, 07MnNiMoDR Material, GB/T 19189, 07MnNiMoDR Steel, 07MnNiMoDR Yield, 07MnNiMoDR plate, 07MnNiMoDR HIC, 07MnNiMoDR NACE MR0175, 07MnNiMoDR ISO 15156, 07MnNiMoDR NACE MR0103, 07MnNiMoDR SSC

Keyword: 07MnNiMoDR,GB/T 19189 07MnNiMoDR,07MnNiMoDR Steel,07MnNiMoDR HIC,07MnNiMoDR NACE

1.  07MnNiMoDR Adopt standard: GB/T 19189Quenched and tempered high strength steel plates for pressure vessels.

2.  07MnNiMoDR Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for 07MnNiMoDR: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  07MnNiMoDR Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | P% | S% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 07MnNiMoDR | 0.09 | 0.15-0.4 | 1.2-1.6 | 0.015 | 0.005 | 0.25 | 0.3-0.6 | 0.30 |
|  | Mo% | V% | B % | Pcm% |  |  |  |  |
|  | 0.1-0.3 | 0.06 | 0.002 | 0.21 |  |  |  |  |

5.  07MnNiMoDR Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| 07MnNiMoDR |  |  |  |  | Degree | Min J |
|  | 10-50 | 490 Mpa | 610-730 Mpa | 17% | -50 | 80J |

6.  Normally GB/T 19189 07MnNiMoDR plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  07MnNiMoDR Delivery Time Or Lead Time: 20-35days

8.  07MnNiMoDR Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for 07MnNiMoDR, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 19189 07MnNiMoDR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

07MnNiMoDR,GB/T 19189 07MnNiMoDR,07MnNiMoDR Steel Plate,07MnNiMoDR HIC,07MnNiMoDR Nace

Tags: 07MnNiMoDR,GB/T 19189 07MnNiMoDR,07MnNiMoDR Steel Plate,07MnNiMoDR steel factory, 07MnNiMoDR adopt standard, 07MnNiMoDR Heat treatment, 07MnNiMoDR Technical delivery condition, 07MnNiMoDR Chemical, 07MnNiMoDR Mechanical property, 07MnNiMoDR Price, 07MnNiMoDR CEV, 07MnNiMoDR Impact degree, 07MnNiMoDR impact energy, 07MnNiMoDR Supplier,07MnNiMoDR Specification, 07MnNiMoDR properties, Material 07MnNiMoDR N, 07MnNiMoDR Material, GB/T 19189, 07MnNiMoDR Steel, 07MnNiMoDR Yield, 07MnNiMoDR plate, 07MnNiMoDR HIC, 07MnNiMoDR NACE MR0175, 07MnNiMoDR ISO 15156, 07MnNiMoDR NACE MR0103, 07MnNiMoDR SSC