GB/T 19189 07MnNiVDR, 07MnNiVDR STEEL PLATE,07MnNiVDR Boiler steel plate

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 19189 07MnNiVDR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,Quenched and tempered high strength steel plates for pressure vessels,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

07MnNiVDR,GB/T 19189 07MnNiVDR,07MnNiVDR Steel Plate,07MnNiVDR HIC,07MnNiVDR Nace

Tags: 07MnNiVDR,GB/T 19189 07MnNiVDR,07MnNiVDR Steel Plate,07MnNiVDR steel factory, 07MnNiVDR adopt standard, 07MnNiVDR Heat treatment, 07MnNiVDR Technical delivery condition, 07MnNiVDR Chemical, 07MnNiVDR Mechanical property, 07MnNiVDR Price, 07MnNiVDR CEV, 07MnNiVDR Impact degree, 07MnNiVDR impact energy, 07MnNiVDR Supplier,07MnNiVDR Specification, 07MnNiVDR properties, Material 07MnNiVDR N, 07MnNiVDR Material, GB/T 19189, 07MnNiVDR Steel, 07MnNiVDR Yield, 07MnNiVDR plate, 07MnNiVDR HIC, 07MnNiVDR NACE MR0175, 07MnNiVDR ISO 15156, 07MnNiVDR NACE MR0103, 07MnNiVDR SSC

Keyword: 07MnNiVDR,GB/T 19189 07MnNiVDR,07MnNiVDR Steel,07MnNiVDR HIC,07MnNiVDR NACE

1.  07MnNiVDR Adopt standard: GB/T 19189Quenched and tempered high strength steel plates for pressure vessels.

2.  07MnNiVDR Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for 07MnNiVDR: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  07MnNiVDR Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | P% | S% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 07MnNiVDR | 0.09 | 0.15-0.4 | 1.2-1.6 | 0.018 | 0.008 | 0.25 | 0.20-0.50 | 0.30 |
|  | Mo% | V% | B % | Pcm% |  |  |  |  |
|  | 0.3 | 0.02-0.06 | 0.002 | 0.21 |  |  |  |  |

5.  07MnNiVDR Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
| 07MnNiVDR |  |  |  |  | Degree | Min J |
|  | 10-60 | 490 Mpa | 610-730 Mpa | 17% | -40 | 80J |

6.  Normally GB/T 19189 07MnNiVDR plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  07MnNiVDR Delivery Time Or Lead Time: 20-35days

8.  07MnNiVDR Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for 07MnNiVDR, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 19189 07MnNiVDR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

07MnNiVDR,GB/T 19189 07MnNiVDR,07MnNiVDR Steel Plate,07MnNiVDR HIC,07MnNiVDR Nace

Tags: 07MnNiVDR,GB/T 19189 07MnNiVDR,07MnNiVDR Steel Plate,07MnNiVDR steel factory, 07MnNiVDR adopt standard, 07MnNiVDR Heat treatment, 07MnNiVDR Technical delivery condition, 07MnNiVDR Chemical, 07MnNiVDR Mechanical property, 07MnNiVDR Price, 07MnNiVDR CEV, 07MnNiVDR Impact degree, 07MnNiVDR impact energy, 07MnNiVDR Supplier,07MnNiVDR Specification, 07MnNiVDR properties, Material 07MnNiVDR N, 07MnNiVDR Material, GB/T 19189, 07MnNiVDR Steel, 07MnNiVDR Yield, 07MnNiVDR plate, 07MnNiVDR HIC, 07MnNiVDR NACE MR0175, 07MnNiVDR ISO 15156, 07MnNiVDR NACE MR0103, 07MnNiVDR SSC