GB/T 713 13MnNiMoR, 13MnNiMoR STEEL PLATE,13MnNiMoR Boiler steel plate

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 713 13MnNiMoR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

13MnNiMoR,GB/T 713 13MnNiMoR,13MnNiMoR Steel Plate,13MnNiMoR HIC,13MnNiMoR Nace

Tags: 13MnNiMoR,GB/T 713 13MnNiMoR,13MnNiMoR Steel Plate,13MnNiMoR steel factory, 13MnNiMoR adopt standard, 13MnNiMoR Heat treatment, 13MnNiMoR Technical delivery condition, 13MnNiMoR Chemical, 13MnNiMoR Mechanical property, 13MnNiMoR Price, 13MnNiMoR CEV, 13MnNiMoR Impact degree, 13MnNiMoR impact energy, 13MnNiMoR Supplier,13MnNiMoR Specification, 13MnNiMoR properties, Material 13MnNiMoR N, 13MnNiMoR Material, GB/T 713, 13MnNiMoR Steel, 13MnNiMoR Yield, 13MnNiMoR plate, 13MnNiMoR HIC, 13MnNiMoR NACE MR0175, 13MnNiMoR ISO 15156, 13MnNiMoR NACE MR0103, 13MnNiMoR SSC

Keyword: 13MnNiMoR,GB/T 713 13MnNiMoR,13MnNiMoR Steel,13MnNiMoR HIC,13MnNiMoR NACE

- 13MnNiMoR Adopt standard: GB/T 713 Standard Specification for boiler and pressure purposes, technical delivery condition and non alloy, alloy steels with specified elevated temperature properties.

- 13MnNiMoR Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for 13MnNiMoR: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- 13MnNiMoR Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | Cu % | Ni % | Cr% | Mo % | V % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13MnNiMoR | 0.15 | 0.15-0.5 | 1.2-1.6 | 0.30 | 0.6-1.0 | 0.2-0.4 | 0.2-0.4 | -- |
|  | Ti % | Alt % | P % | S % | Nb |  |  |  |
|  | -- | -- | 0.02 | 0.01 | 0.005-0.02 |  |  |  |

- 13MnNiMoR Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Degree | Min J |
| 13MnNiMoR | 30-100 | 390 Mpa | 570-720 Mpa | 18% | 0 | 47J |
|  | 100-150 | 380 Mpa | 570-720 Mpa | 18% | 0 | 47J |

Normally GB/T 713 13MnNiMoR plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

- 13MnNiMoR Delivery Time Or Lead Time: 20-35days

- 13MnNiMoR Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for 13MnNiMoR, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 713 13MnNiMoR NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

13MnNiMoR,GB/T 713 13MnNiMoR,13MnNiMoR Steel Plate,13MnNiMoR HIC,13MnNiMoR Nace

Tags: 13MnNiMoR,GB/T 713 13MnNiMoR,13MnNiMoR Steel Plate,13MnNiMoR steel factory, 13MnNiMoR adopt standard, 13MnNiMoR Heat treatment, 13MnNiMoR Technical delivery condition, 13MnNiMoR Chemical, 13MnNiMoR Mechanical property, 13MnNiMoR Price, 13MnNiMoR CEV, 13MnNiMoR Impact degree, 13MnNiMoR impact energy, 13MnNiMoR Supplier,13MnNiMoR Specification, 13MnNiMoR properties, Material 13MnNiMoR N, 13MnNiMoR Material, GB/T 713, 13MnNiMoR Steel, 13MnNiMoR Yield, 13MnNiMoR plate, 13MnNiMoR HIC, 13MnNiMoR NACE MR0175, 13MnNiMoR ISO 15156, 13MnNiMoR NACE MR0103, 13MnNiMoR SSC