A387GR21,A387GR21 Steel Plate,A387GR21 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR21 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. A387GR21,A387/A387M A387GR21,A387GR21 Steel Plate,A387GR21 HIC,A387GR21 Nace

Tags: A387GR21,A387/A387M A387GR21,A387GR21 Steel Plate,A387GR21 steel factory, A387GR21 adopt standard, A387GR21 Heat treatment, A387GR21 Technical delivery condition, A387GR21 Chemical, A387GR21 Mechanical property, A387GR21 Price, A387GR21 CEV, A387GR21 Impact degree, A387GR21 impact energy, A387GR21 Supplier,A387GR21 Specification, A387GR21 properties, Material A387GR21 N, A387GR21 Material, A387/A387M, A387GR21 Steel, A387GR21 Yield, A387GR21 plate, A387GR21 HIC, A387GR21 NACE MR0175, A387GR21 ISO 15156, A387GR21 NACE MR0103, A387GR21 SSC

Keyword: A387GR21,A387GR21 Steel Plate,A387GR21 Supplier

1.  A387GR21 Adopt standard: ASMT A387/A387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  A387GR21 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A387GR21: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A387GR21 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387GR21 | 0.04-0.15 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 2.63-3.37 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  A387GR21 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A387GR21 | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally A387/A387M A387GR21 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A387GR21 Delivery Time Or Lead Time: 20-35days

8.  A387GR21 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A387GR21, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR21 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A387GR21,A387/A387M A387GR21,A387GR21 Steel Plate,A387GR21 HIC,A387GR21 Nace

Tags: A387GR21,A387/A387M A387GR21,A387GR21 Steel Plate,A387GR21 steel factory, A387GR21 adopt standard, A387GR21 Heat treatment, A387GR21 Technical delivery condition, A387GR21 Chemical, A387GR21 Mechanical property, A387GR21 Price, A387GR21 CEV, A387GR21 Impact degree, A387GR21 impact energy, A387GR21 Supplier,A387GR21 Specification, A387GR21 properties, Material A387GR21 N, A387GR21 Material, A387/A387M, A387GR21 Steel, A387GR21 Yield, A387GR21 plate, A387GR21 HIC, A387GR21 NACE MR0175, A387GR21 ISO 15156, A387GR21 NACE MR0103, A387GR21 SSC