A387GR22,A387GR22 Steel Plate,A387GR22 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR22 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. A387GR22,A387/A387M A387GR22,A387GR22 Steel Plate,A387GR22 HIC,A387GR22 Nace

Tags: A387GR22,A387/A387M A387GR22,A387GR22 Steel Plate,A387GR22 steel factory, A387GR22 adopt standard, A387GR22 Heat treatment, A387GR22 Technical delivery condition, A387GR22 Chemical, A387GR22 Mechanical property, A387GR22 Price, A387GR22 CEV, A387GR22 Impact degree, A387GR22 impact energy, A387GR22 Supplier,A387GR22 Specification, A387GR22 properties, Material A387GR22 N, A387GR22 Material, A387/A387M, A387GR22 Steel, A387GR22 Yield, A387GR22 plate, A387GR22 HIC, A387GR22 NACE MR0175, A387GR22 ISO 15156, A387GR22 NACE MR0103, A387GR22 SSC

Keyword: A387GR22,A387GR22 Steel Plate,A387GR22 Supplier

1.  A387GR22 Adopt standard: ASMT A387/A387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  A387GR22 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A387GR22: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A387GR22 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387GR22 | 0.04-0.15 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 1.88-2.62 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  A387GR22 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A387GR22 | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally A387/A387M A387GR22 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A387GR22 Delivery Time Or Lead Time: 20-35days

8.  A387GR22 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A387GR22, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR22 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A387GR22,A387/A387M A387GR22,A387GR22 Steel Plate,A387GR22 HIC,A387GR22 Nace

Tags: A387GR22,A387/A387M A387GR22,A387GR22 Steel Plate,A387GR22 steel factory, A387GR22 adopt standard, A387GR22 Heat treatment, A387GR22 Technical delivery condition, A387GR22 Chemical, A387GR22 Mechanical property, A387GR22 Price, A387GR22 CEV, A387GR22 Impact degree, A387GR22 impact energy, A387GR22 Supplier,A387GR22 Specification, A387GR22 properties, Material A387GR22 N, A387GR22 Material, A387/A387M, A387GR22 Steel, A387GR22 Yield, A387GR22 plate, A387GR22 HIC, A387GR22 NACE MR0175, A387GR22 ISO 15156, A387GR22 NACE MR0103, A387GR22 SSC