A387GR22L,A387GR22L Steel Plate,A387GR22L Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR22L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. A387GR22L,A387/A387M A387GR22L,A387GR22L Steel Plate,A387GR22L HIC,A387GR22L Nace

Tags: A387GR22L,A387/A387M A387GR22L,A387GR22L Steel Plate,A387GR22L steel factory, A387GR22L adopt standard, A387GR22L Heat treatment, A387GR22L Technical delivery condition, A387GR22L Chemical, A387GR22L Mechanical property, A387GR22L Price, A387GR22L CEV, A387GR22L Impact degree, A387GR22L impact energy, A387GR22L Supplier,A387GR22L Specification, A387GR22L properties, Material A387GR22L N, A387GR22L Material, A387/A387M, A387GR22L Steel, A387GR22L Yield, A387GR22L plate, A387GR22L HIC, A387GR22L NACE MR0175, A387GR22L ISO 15156, A387GR22L NACE MR0103, A387GR22L SSC

Keyword: A387GR22L,A387GR22L Steel Plate,A387GR22L Supplier

1.  A387GR22L Adopt standard: ASMT A387/A387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  A387GR22L Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A387GR22L: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A387GR22L Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A387GR22L | 0.12 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 1.88-2.62 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  A387GR22L Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A387GR22L | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally A387/A387M A387GR22L plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A387GR22L Delivery Time Or Lead Time: 20-35days

8.  A387GR22L Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A387GR22L, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A387/A387M A387GR22L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A387GR22L,A387/A387M A387GR22L,A387GR22L Steel Plate,A387GR22L HIC,A387GR22L Nace

Tags: A387GR22L,A387/A387M A387GR22L,A387GR22L Steel Plate,A387GR22L steel factory, A387GR22L adopt standard, A387GR22L Heat treatment, A387GR22L Technical delivery condition, A387GR22L Chemical, A387GR22L Mechanical property, A387GR22L Price, A387GR22L CEV, A387GR22L Impact degree, A387GR22L impact energy, A387GR22L Supplier,A387GR22L Specification, A387GR22L properties, Material A387GR22L N, A387GR22L Material, A387/A387M, A387GR22L Steel, A387GR22L Yield, A387GR22L plate, A387GR22L HIC, A387GR22L NACE MR0175, A387GR22L ISO 15156, A387GR22L NACE MR0103, A387GR22L SSC