SA529GR55,SA529GR55 Steel Plate,SA529GR55 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA 529/SA 529M SA529GR55 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for High-Strength Carbon-Manganese Steel of Structural Quality Which is a large steel plate supplier mill at Gangsteel Group. SA529GR55,SA 529/SA 529M SA529GR55,SA529GR55 Steel Plate,SA529GR55 HIC,SA529GR55 Nace

Tags: SA529GR55,SA 529/SA 529M SA529GR55,SA529GR55 Steel Plate,SA529GR55 steel factory, SA529GR55 adopt standard, SA529GR55 Heat treatment, SA529GR55 Technical delivery condition, SA529GR55 Chemical, SA529GR55 Mechanical property, SA529GR55 Price, SA529GR55 CEV, SA529GR55 Impact degree, SA529GR55 impact energy, SA529GR55 Supplier,SA529GR55 Specification, SA529GR55 properties, Material SA529GR55 N, SA529GR55 Material, SA 529/SA 529M, SA529GR55 Steel, SA529GR55 Yield, SA529GR55 plate, SA529GR55 HIC, SA529GR55 NACE MR0175, SA529GR55 ISO 15156, SA529GR55 NACE MR0103, SA529GR55 SSC

Keyword: SA529GR55,SA529GR55 Steel Plate,SA529GR55 Supplier

1.  SA529GR55 Adopt standard: ASME SA 529/SA 529M Standard Specification for High-Strength Carbon-Manganese Steel of Structural Quality

2.  SA529GR55 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA529GR55: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA529GR55 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cu% |
| --- | --- | --- | --- | --- | --- | --- |
| SA529GR55 | 0.27 | 1.35 | 0.04 | 0.05 | 0.40 | 0.20 |

5.  SA529GR55 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA529GR55 | 380Mpa(min) | 485Mpa(min) | 200mm | -- |
|  | 380Mpa(min) | 690Mpa（max） | 50mm | -- |

6.  Normally SA 529/SA 529M SA529GR55 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA529GR55 Delivery Time Or Lead Time: 20-35days

8.  SA529GR55 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA529GR55, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA 529/SA 529M SA529GR55 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA529GR55,SA 529/SA 529M SA529GR55,SA529GR55 Steel Plate,SA529GR55 HIC,SA529GR55 Nace

Tags: SA529GR55,SA 529/SA 529M SA529GR55,SA529GR55 Steel Plate,SA529GR55 steel factory, SA529GR55 adopt standard, SA529GR55 Heat treatment, SA529GR55 Technical delivery condition, SA529GR55 Chemical, SA529GR55 Mechanical property, SA529GR55 Price, SA529GR55 CEV, SA529GR55 Impact degree, SA529GR55 impact energy, SA529GR55 Supplier,SA529GR55 Specification, SA529GR55 properties, Material SA529GR55 N, SA529GR55 Material, SA 529/SA 529M, SA529GR55 Steel, SA529GR55 Yield, SA529GR55 plate, SA529GR55 HIC, SA529GR55 NACE MR0175, SA529GR55 ISO 15156, SA529GR55 NACE MR0103, SA529GR55 SSC