A533 TYPE A,A533 TYPE A Steel Plate,A533 TYPE A Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A533/A533M A533 TYPE A NACE MR0175, MR0103 Boiler steel plate, Standard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel Which is a large steel plate supplier mill at Gangsteel Group. A533 TYPE A,A533/A533M A533 TYPE A,A533 TYPE A Steel Plate,A533 TYPE A HIC,A533 TYPE A Nace

Tags: A533 TYPE A,A533/A533M A533 TYPE A,A533 TYPE A Steel Plate,A533 TYPE A steel factory, A533 TYPE A adopt standard, A533 TYPE A Heat treatment, A533 TYPE A Technical delivery condition, A533 TYPE A Chemical, A533 TYPE A Mechanical property, A533 TYPE A Price, A533 TYPE A CEV, A533 TYPE A Impact degree, A533 TYPE A impact energy, A533 TYPE A Supplier,A533 TYPE A Specification, A533 TYPE A properties, Material A533 TYPE A N, A533 TYPE A Material, A533/A533M, A533 TYPE A Steel, A533 TYPE A Yield, A533 TYPE A plate, A533 TYPE A HIC, A533 TYPE A NACE MR0175, A533 TYPE A ISO 15156, A533 TYPE A NACE MR0103, A533 TYPE A SSC

Keyword: A533 TYPE A,A533 TYPE A Steel Plate,A533 TYPE A Supplier

1.  A533 TYPE A Adopt standard: ASMT A533/A533MStandard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel

2.  A533 TYPE A Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A533 TYPE A: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A533 TYPE A Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| A533 TYPE A | 0.25 | 1.07-1.82 | 0.035 | 0.035 | 0.13-0.45 | 0.41-0.84 | -- |

5.  A533 TYPE A Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A533 TYPE A | 345 Mpa | 550-690Mpa | <50MM | 18% |

6.  Normally A533/A533M A533 TYPE A plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A533 TYPE A Delivery Time Or Lead Time: 20-35days

8.  A533 TYPE A Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A533 TYPE A, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A533/A533MA533 TYPE A NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A533 TYPE A,A533/A533M A533 TYPE A,A533 TYPE A Steel Plate,A533 TYPE A HIC,A533 TYPE A Nace

Tags: A533 TYPE A,A533/A533M A533 TYPE A,A533 TYPE A Steel Plate,A533 TYPE A steel factory, A533 TYPE A adopt standard, A533 TYPE A Heat treatment, A533 TYPE A Technical delivery condition, A533 TYPE A Chemical, A533 TYPE A Mechanical property, A533 TYPE A Price, A533 TYPE A CEV, A533 TYPE A Impact degree, A533 TYPE A impact energy, A533 TYPE A Supplier,A533 TYPE A Specification, A533 TYPE A properties, Material A533 TYPE A N, A533 TYPE A Material, A533/A533M, A533 TYPE A Steel, A533 TYPE A Yield, A533 TYPE A plate, A533 TYPE A HIC, A533 TYPE A NACE MR0175, A533 TYPE A ISO 15156, A533 TYPE A NACE MR0103, A533 TYPE A SSC