A710 CLASS 2,A710 CLASS 2 Steel Plate,A710 CLASS 2 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710M A710 CLASS 2 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. A710 CLASS 2,A710/A710M A710 CLASS 2,A710 CLASS 2 Steel Plate,A710 CLASS 2 HIC,A710 CLASS 2 Nace

Tags: A710 CLASS 2,A710/A710M A710 CLASS 2,A710 CLASS 2 Steel Plate,A710 CLASS 2 steel factory, A710 CLASS 2 adopt standard, A710 CLASS 2 Heat treatment, A710 CLASS 2 Technical delivery condition, A710 CLASS 2 Chemical, A710 CLASS 2 Mechanical property, A710 CLASS 2 Price, A710 CLASS 2 CEV, A710 CLASS 2 Impact degree, A710 CLASS 2 impact energy, A710 CLASS 2 Supplier,A710 CLASS 2 Specification, A710 CLASS 2 properties, Material A710 CLASS 2 N, A710 CLASS 2 Material, A710/A710M, A710 CLASS 2 Steel, A710 CLASS 2 Yield, A710 CLASS 2 plate, A710 CLASS 2 HIC, A710 CLASS 2 NACE MR0175, A710 CLASS 2 ISO 15156, A710 CLASS 2 NACE MR0103, A710 CLASS 2 SSC

Keyword: A710 CLASS 2,A710 CLASS 2 Steel Plate,A710 CLASS 2 Supplier

1.  A710 CLASS 2 Adopt standard: ASMT A710/A710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  A710 CLASS 2 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A710 CLASS 2: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A710 CLASS 2 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| A710 CLASS 2 | 0.07 | 0.40-0.70 | 0.025 | 0.025 | 0.4 | 0.7-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.15-0.25 | 1.0-1.3 | 0.02 | -- | 0.6-0.9 |  |

5.  A710 CLASS 2 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A710 CLASS 2 | 450Mpa | 495Mpa | <6.5mm | 20% |
|  | 450Mpa | 495Mpa | 6.5-8mm | 20% |
|  | 450Mpa | 495Mpa | 8-10mm | 20% |
|  | 450Mpa | 495Mpa | 10-12.5mm | 20% |
|  | 450Mpa | 495Mpa | 12.5-20mm | 20% |
|  | 450 Mpa | 495Mpa | 20-25mm | 20% |
|  | 415 Mpa | 495Mpa | 25-30mm | 20% |
|  | 415 Mpa | 495Mpa | 30-50mm | 20% |
|  | 380Mpa | 450Mpa | 50-100mm | -- |
|  | 345Mpa | 415Mpa | >100mm | -- |

6.  Normally A710/A710M A710 CLASS 2 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A710 CLASS 2 Delivery Time Or Lead Time: 20-35days

8.  A710 CLASS 2 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A710 CLASS 2, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting A710/A710MA710 CLASS 2 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A710 CLASS 2,A710/A710M A710 CLASS 2,A710 CLASS 2 Steel Plate,A710 CLASS 2 HIC,A710 CLASS 2 Nace

Tags: A710 CLASS 2,A710/A710M A710 CLASS 2,A710 CLASS 2 Steel Plate,A710 CLASS 2 steel factory, A710 CLASS 2 adopt standard, A710 CLASS 2 Heat treatment, A710 CLASS 2 Technical delivery condition, A710 CLASS 2 Chemical, A710 CLASS 2 Mechanical property, A710 CLASS 2 Price, A710 CLASS 2 CEV, A710 CLASS 2 Impact degree, A710 CLASS 2 impact energy, A710 CLASS 2 Supplier,A710 CLASS 2 Specification, A710 CLASS 2 properties, Material A710 CLASS 2 N, A710 CLASS 2 Material, A710/A710M, A710 CLASS 2 Steel, A710 CLASS 2 Yield, A710 CLASS 2 plate, A710 CLASS 2 HIC, A710 CLASS 2 NACE MR0175, A710 CLASS 2 ISO 15156, A710 CLASS 2 NACE MR0103, A710 CLASS 2 SSC