A841GRD,A841GRD Steel Plate,A841GRD Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841GRD NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. A841GRD,SA-841/SA-841M A841GRD,A841GRD Steel Plate,A841GRD HIC,A841GRD Nace

Tags: A841GRD,SA-841/SA-841M A841GRD,A841GRD Steel Plate,A841GRD steel factory, A841GRD adopt standard, A841GRD Heat treatment, A841GRD Technical delivery condition, A841GRD Chemical, A841GRD Mechanical property, A841GRD Price, A841GRD CEV, A841GRD Impact degree, A841GRD impact energy, A841GRD Supplier,A841GRD Specification, A841GRD properties, Material A841GRD N, A841GRD Material, SA-841/SA-841M, A841GRD Steel, A841GRD Yield, A841GRD plate, A841GRD HIC, A841GRD NACE MR0175, A841GRD ISO 15156, A841GRD NACE MR0103, A841GRD SSC

Keyword: A841GRD,A841GRD Steel Plate,A841GRD Supplier

1.  A841GRD Adopt standard: ASMT SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  A841GRD Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for A841GRD: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  A841GRD Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A841GRD | 0.09 | 1.0-2.0 | 0.01 | 0.005 | 0.05-0.25 | 0.5 | 1.0-5.0 | 0.3 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.4 | 0.05 | 0.02 | -- | 0.006-0.03 | 0.0005-0.002 |  |  |

5.  A841GRD Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| A841GRD | 690 Mpa | 1000-1170Mpa | <40MM | 13% |
|  | -- | -- | 40-65MM | -- |
|  | -- | -- | >65MM | -- |

6.  Normally SA-841/SA-841M A841GRD plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  A841GRD Delivery Time Or Lead Time: 20-35days

8.  A841GRD Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for A841GRD, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M A841GRD NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. A841GRD,SA-841/SA-841M A841GRD,A841GRD Steel Plate,A841GRD HIC,A841GRD Nace

Tags: A841GRD,SA-841/SA-841M A841GRD,A841GRD Steel Plate,A841GRD steel factory, A841GRD adopt standard, A841GRD Heat treatment, A841GRD Technical delivery condition, A841GRD Chemical, A841GRD Mechanical property, A841GRD Price, A841GRD CEV, A841GRD Impact degree, A841GRD impact energy, A841GRD Supplier,A841GRD Specification, A841GRD properties, Material A841GRD N, A841GRD Material, SA-841/SA-841M, A841GRD Steel, A841GRD Yield, A841GRD plate, A841GRD HIC, A841GRD NACE MR0175, A841GRD ISO 15156, A841GRD NACE MR0103, A841GRD SSC