GB/T 713 Q370R, Q370R STEEL PLATE,Q370R Boiler steel plate

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 713 Q370R NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

Q370R,GB/T 713 Q370R,Q370R Steel Plate,Q370R HIC,Q370R Nace

Tags: Q370R,GB/T 713 Q370R,Q370R Steel Plate,Q370R steel factory, Q370R adopt standard, Q370R Heat treatment, Q370R Technical delivery condition, Q370R Chemical, Q370R Mechanical property, Q370R Price, Q370R CEV, Q370R Impact degree, Q370R impact energy, Q370R Supplier,Q370R Specification, Q370R properties, Material Q370R N, Q370R Material, GB/T 713, Q370R Steel, Q370R Yield, Q370R plate, Q370R HIC, Q370R NACE MR0175, Q370R ISO 15156, Q370R NACE MR0103, Q370R SSC

Keyword: Q370R,GB/T 713 Q370R,Q370R Steel,Q370R HIC,Q370R NACE

- Q370R Adopt standard: GB/T 713 Standard Specification for boiler and pressure purposes, technical delivery condition and non alloy, alloy steels with specified elevated temperature properties.

- Q370R Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

- Third Party Inspection for Q370R: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

- Q370R Chemical composition % of the Product analysis of grade

| Grade | C % | Si % | Mn % | Cu % | Ni % | Cr% | Mo % | V % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Q370R | 0.18 | 0.55 | 1.2-.1.7 | 0.3 | 0.3 | 0.3 | 0.08 | 0.05 |
|  | Ti % | Alt % | P % | S % | Nb |  |  |  |
|  | 0.03 | 0.02 | 0.025 | 0.010 | 0.015-0.05 |  |  |  |

- Q370R Mechanical Property

| Grade | Thickness(mm) | Min Yield | Tensile | Elongation | Min Impact Energy |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Degree | Min J |
| Q370R | 10-16 | 370Mpa | 530-630 Mpa | 20% | -20 | 47J |
|  | 16-36 | 360 Mpa | 530-630 Mpa | 20% | -20 | 47J |
|  | 36-60 | 340 Mpa | 520-620 Mpa | 20% | -20 | 47J |
|  | 60-100 | 330 Mpa | 510-610 Mpa | 20% | -20 | 47J |

Normally GB/T 713 Q370R plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

- Q370R Delivery Time Or Lead Time: 20-35days

- Q370R Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

- If you have any requirement in steel plate for Q370R, whether the new plate or stock list of material, please feel free to contact us by email of calling.

- If you had any question at our plate or service. Please contact our after service department to get faster reply.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting GB/T 713 Q370R NACE MR0175, MR0103 Boiler steel plate, Low alloy and high strength steel plate,                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                  heavy plate and wide, heavy plate, Which is a large steel plate supplier mill at Gangsteel Group.

Q370R,GB/T 713 Q370R,Q370R Steel Plate,Q370R HIC,Q370R Nace

Tags: Q370R,GB/T 713 Q370R,Q370R Steel Plate,Q370R steel factory, Q370R adopt standard, Q370R Heat treatment, Q370R Technical delivery condition, Q370R Chemical, Q370R Mechanical property, Q370R Price, Q370R CEV, Q370R Impact degree, Q370R impact energy, Q370R Supplier,Q370R Specification, Q370R properties, Material Q370R N, Q370R Material, GB/T 713, Q370R Steel, Q370R Yield, Q370R plate, Q370R HIC, Q370R NACE MR0175, Q370R ISO 15156, Q370R NACE MR0103, Q370R SSC