SA202GRA,SA202GRA Steel Plate,SA202GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA202/SA202M SA202GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA202GRA,SA202/SA202M SA202GRA,SA202GRA Steel Plate,SA202GRA HIC,SA202GRA Nace

Tags: SA202GRA,SA202/SA202M SA202GRA,SA202GRA Steel Plate,SA202GRA steel factory, SA202GRA adopt standard, SA202GRA Heat treatment, SA202GRA Technical delivery condition, SA202GRA Chemical, SA202GRA Mechanical property, SA202GRA Price, SA202GRA CEV, SA202GRA Impact degree, SA202GRA impact energy, SA202GRA Supplier,SA202GRA Specification, SA202GRA properties, Material SA202GRA N, SA202GRA Material, SA202/SA202M, SA202GRA Steel, SA202GRA Yield, SA202GRA plate, SA202GRA HIC, SA202GRA NACE MR0175, SA202GRA ISO 15156, SA202GRA NACE MR0103, SA202GRA SSC

Keyword: SA202GRA,SA202GRA Steel Plate,SA202GRA Supplier

1.  SA202GRA Adopt standard: ASME SA202/SA202M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  SA202GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA202GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA202GRA Chemical composition % of the Product analysis of grade

| Grade | C % | P % | S% | Si% | Cr% | Mn% |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA202GRA | 0.17 | 0.035 | 0.035 | 0.54-0.96 | 0.31-0.64 | 0.97-1.52 |  |  |

5.  SA202GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA202GRA | 310 Mpa | 515-655Mpa | <=50MM | 19% |
|  | 310 Mpa | 515-655Mpa | 50-200MM | 16% |

6.  Normally SA202/SA202M SA202GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA202GRA Delivery Time Or Lead Time: 20-35days

8.  SA202GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA202GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA202/SA202M SA202GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA202GRA,SA202/SA202M SA202GRA,SA202GRA Steel Plate,SA202GRA HIC,SA202GRA Nace

Tags: SA202GRA,SA202/SA202M SA202GRA,SA202GRA Steel Plate,SA202GRA steel factory, SA202GRA adopt standard, SA202GRA Heat treatment, SA202GRA Technical delivery condition, SA202GRA Chemical, SA202GRA Mechanical property, SA202GRA Price, SA202GRA CEV, SA202GRA Impact degree, SA202GRA impact energy, SA202GRA Supplier,SA202GRA Specification, SA202GRA properties, Material SA202GRA N, SA202GRA Material, SA202/SA202M, SA202GRA Steel, SA202GRA Yield, SA202GRA plate, SA202GRA HIC, SA202GRA NACE MR0175, SA202GRA ISO 15156, SA202GRA NACE MR0103, SA202GRA SSC