SA202GRB,SA202GRB Steel Plate,SA202GRB Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA202/SA202M SA202GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA202GRB,SA202/SA202M SA202GRB,SA202GRB Steel Plate,SA202GRB HIC,SA202GRB Nace

Tags: SA202GRB,SA202/SA202M SA202GRB,SA202GRB Steel Plate,SA202GRB steel factory, SA202GRB adopt standard, SA202GRB Heat treatment, SA202GRB Technical delivery condition, SA202GRB Chemical, SA202GRB Mechanical property, SA202GRB Price, SA202GRB CEV, SA202GRB Impact degree, SA202GRB impact energy, SA202GRB Supplier,SA202GRB Specification, SA202GRB properties, Material SA202GRB N, SA202GRB Material, SA202/SA202M, SA202GRB Steel, SA202GRB Yield, SA202GRB plate, SA202GRB HIC, SA202GRB NACE MR0175, SA202GRB ISO 15156, SA202GRB NACE MR0103, SA202GRB SSC

Keyword: SA202GRB,SA202GRB Steel Plate,SA202GRB Supplier

1.  SA202GRB Adopt standard: ASME SA202/SA202M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  SA202GRB Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA202GRB: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA202GRB Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | Si% | Cr% |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA202GRB | 0.25 | 0.97-1.52 | 0.035 | 0.54-0.96 | 0.31-0.64 |  |  |  |

5.  SA202GRB Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA202GRB | 325 Mpa | 585-760Mpa | <=50MM | 18% |
|  | 325 Mpa | 585-760Mpa | 50-200MM | 15% |

6.  Normally SA202/SA202M SA202GRB plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA202GRB Delivery Time Or Lead Time: 20-35days

8.  SA202GRB Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA202GRB, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA202/SA202M SA202GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA202GRB,SA202/SA202M SA202GRB,SA202GRB Steel Plate,SA202GRB HIC,SA202GRB Nace

Tags: SA202GRB,SA202/SA202M SA202GRB,SA202GRB Steel Plate,SA202GRB steel factory, SA202GRB adopt standard, SA202GRB Heat treatment, SA202GRB Technical delivery condition, SA202GRB Chemical, SA202GRB Mechanical property, SA202GRB Price, SA202GRB CEV, SA202GRB Impact degree, SA202GRB impact energy, SA202GRB Supplier,SA202GRB Specification, SA202GRB properties, Material SA202GRB N, SA202GRB Material, SA202/SA202M, SA202GRB Steel, SA202GRB Yield, SA202GRB plate, SA202GRB HIC, SA202GRB NACE MR0175, SA202GRB ISO 15156, SA202GRB NACE MR0103, SA202GRB SSC