SA283GRA,SA283GRA Steel Plate,SA283GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRA,SA283/SA283M SA283GRA,SA283GRA Steel Plate,SA283GRA HIC,SA283GRA Nace

Tags: SA283GRA,SA283/SA283M SA283GRA,SA283GRA Steel Plate,SA283GRA steel factory, SA283GRA adopt standard, SA283GRA Heat treatment, SA283GRA Technical delivery condition, SA283GRA Chemical, SA283GRA Mechanical property, SA283GRA Price, SA283GRA CEV, SA283GRA Impact degree, SA283GRA impact energy, SA283GRA Supplier,SA283GRA Specification, SA283GRA properties, Material SA283GRA N, SA283GRA Material, SA283/SA283M, SA283GRA Steel, SA283GRA Yield, SA283GRA plate, SA283GRA HIC, SA283GRA NACE MR0175, SA283GRA ISO 15156, SA283GRA NACE MR0103, SA283GRA SSC

Keyword: SA283GRA,SA283GRA Steel Plate,SA283GRA Supplier

1.  SA283GRA Adopt standard: ASME SA283/SA283M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  SA283GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA283GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA283GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Cu%(min) | Cu%(<=40mm) | Cu%(>40mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SA283GRA | 0.14 | 0.9 | 0.035 | 0.04 | 0.2 | 0.4 | 0.15-0.4 |

5.  SA283GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA283GRA | 165 Mpa | 301-450Mpa | <=50MM | 30% |
|  | 165Mpa | 310-415Mpa | 50-200MM | 27% |

6.  Normally SA283/SA283M SA283GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA283GRA Delivery Time Or Lead Time: 20-35days

8.  SA283GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA283GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRA,SA283/SA283M SA283GRA,SA283GRA Steel Plate,SA283GRA HIC,SA283GRA Nace

Tags: SA283GRA,SA283/SA283M SA283GRA,SA283GRA Steel Plate,SA283GRA steel factory, SA283GRA adopt standard, SA283GRA Heat treatment, SA283GRA Technical delivery condition, SA283GRA Chemical, SA283GRA Mechanical property, SA283GRA Price, SA283GRA CEV, SA283GRA Impact degree, SA283GRA impact energy, SA283GRA Supplier,SA283GRA Specification, SA283GRA properties, Material SA283GRA N, SA283GRA Material, SA283/SA283M, SA283GRA Steel, SA283GRA Yield, SA283GRA plate, SA283GRA HIC, SA283GRA NACE MR0175, SA283GRA ISO 15156, SA283GRA NACE MR0103, SA283GRA SSC