SA283GRC,SA283GRC Steel Plate,SA283GRC Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRC NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRC,SA283/SA283M SA283GRC,SA283GRC Steel Plate,SA283GRC HIC,SA283GRC Nace

Tags: SA283GRC,SA283/SA283M SA283GRC,SA283GRC Steel Plate,SA283GRC steel factory, SA283GRC adopt standard, SA283GRC Heat treatment, SA283GRC Technical delivery condition, SA283GRC Chemical, SA283GRC Mechanical property, SA283GRC Price, SA283GRC CEV, SA283GRC Impact degree, SA283GRC impact energy, SA283GRC Supplier,SA283GRC Specification, SA283GRC properties, Material SA283GRC N, SA283GRC Material, SA283/SA283M, SA283GRC Steel, SA283GRC Yield, SA283GRC plate, SA283GRC HIC, SA283GRC NACE MR0175, SA283GRC ISO 15156, SA283GRC NACE MR0103, SA283GRC SSC

Keyword: SA283GRC,SA283GRC Steel Plate,SA283GRC Supplier

1.  SA283GRC Adopt standard: ASME SA283/SA283M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  SA283GRC Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA283GRC: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA283GRC Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Cu%(min) | Cu%(<=40mm) | Cu%(>40mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SA283GRC | 0.24 | 0.9 | 0.035 | 0.04 | 0.2 | 0.4 | 0.15-0.4 |

5.  SA283GRC Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA283GRC | 205 Mpa | 380-515Mpa | <=50MM | 25% |
|  | 205Mpa | 380-515Mpa | 50-200MM | 22% |

6.  Normally SA283/SA283M SA283GRC plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA283GRC Delivery Time Or Lead Time: 20-35days

8.  SA283GRC Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA283GRC, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRC NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRC,SA283/SA283M SA283GRC,SA283GRC Steel Plate,SA283GRC HIC,SA283GRC Nace

Tags: SA283GRC,SA283/SA283M SA283GRC,SA283GRC Steel Plate,SA283GRC steel factory, SA283GRC adopt standard, SA283GRC Heat treatment, SA283GRC Technical delivery condition, SA283GRC Chemical, SA283GRC Mechanical property, SA283GRC Price, SA283GRC CEV, SA283GRC Impact degree, SA283GRC impact energy, SA283GRC Supplier,SA283GRC Specification, SA283GRC properties, Material SA283GRC N, SA283GRC Material, SA283/SA283M, SA283GRC Steel, SA283GRC Yield, SA283GRC plate, SA283GRC HIC, SA283GRC NACE MR0175, SA283GRC ISO 15156, SA283GRC NACE MR0103, SA283GRC SSC