SA283GRD,SA283GRD Steel Plate,SA283GRD Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRD NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRD,SA283/SA283M SA283GRD,SA283GRD Steel Plate,SA283GRD HIC,SA283GRD Nace

Tags: SA283GRD,SA283/SA283M SA283GRD,SA283GRD Steel Plate,SA283GRD steel factory, SA283GRD adopt standard, SA283GRD Heat treatment, SA283GRD Technical delivery condition, SA283GRD Chemical, SA283GRD Mechanical property, SA283GRD Price, SA283GRD CEV, SA283GRD Impact degree, SA283GRD impact energy, SA283GRD Supplier,SA283GRD Specification, SA283GRD properties, Material SA283GRD N, SA283GRD Material, SA283/SA283M, SA283GRD Steel, SA283GRD Yield, SA283GRD plate, SA283GRD HIC, SA283GRD NACE MR0175, SA283GRD ISO 15156, SA283GRD NACE MR0103, SA283GRD SSC

Keyword: SA283GRD,SA283GRD Steel Plate,SA283GRD Supplier

1.  SA283GRD Adopt standard: ASME SA283/SA283M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon

2.  SA283GRD Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA283GRD: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA283GRD Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Cu%(min) | Cu%(<=40mm) | Cu%(>40mm) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SA283GRD | 0.27 | 0.9 | 0.035 | 0.04 | 0.2 | 0.4 | 0.15-0.4 |

5.  SA283GRD Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA283GRD | 230 Mpa | 415-550Mpa | <=50MM | 23% |
|  | 230 Mpa | 415-550Mpa | 50-200MM | 20% |

6.  Normally SA283/SA283M SA283GRD plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA283GRD Delivery Time Or Lead Time: 20-35days

8.  SA283GRD Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA283GRD, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA283/SA283M SA283GRD NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA283GRD,SA283/SA283M SA283GRD,SA283GRD Steel Plate,SA283GRD HIC,SA283GRD Nace

Tags: SA283GRD,SA283/SA283M SA283GRD,SA283GRD Steel Plate,SA283GRD steel factory, SA283GRD adopt standard, SA283GRD Heat treatment, SA283GRD Technical delivery condition, SA283GRD Chemical, SA283GRD Mechanical property, SA283GRD Price, SA283GRD CEV, SA283GRD Impact degree, SA283GRD impact energy, SA283GRD Supplier,SA283GRD Specification, SA283GRD properties, Material SA283GRD N, SA283GRD Material, SA283/SA283M, SA283GRD Steel, SA283GRD Yield, SA283GRD plate, SA283GRD HIC, SA283GRD NACE MR0175, SA283GRD ISO 15156, SA283GRD NACE MR0103, SA283GRD SSC