SA387-21L,SA387-21L Steel Plate,SA387-21L Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387-21L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. SA387-21L,SA387/SA387M SA387-21L,SA387-21L Steel Plate,SA387-21L HIC,SA387-21L Nace

Tags: SA387-21L,SA387/SA387M SA387-21L,SA387-21L Steel Plate,SA387-21L steel factory, SA387-21L adopt standard, SA387-21L Heat treatment, SA387-21L Technical delivery condition, SA387-21L Chemical, SA387-21L Mechanical property, SA387-21L Price, SA387-21L CEV, SA387-21L Impact degree, SA387-21L impact energy, SA387-21L Supplier,SA387-21L Specification, SA387-21L properties, Material SA387-21L N, SA387-21L Material, SA387/SA387M, SA387-21L Steel, SA387-21L Yield, SA387-21L plate, SA387-21L HIC, SA387-21L NACE MR0175, SA387-21L ISO 15156, SA387-21L NACE MR0103, SA387-21L SSC

Keyword: SA387-21L,SA387-21L Steel Plate,SA387-21L Supplier

1.  SA387-21L Adopt standard: ASME SA387/SA387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  SA387-21L Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA387-21L: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA387-21L Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA387-21L | 0.12 | 0.25-0.66 | 0.035 | 0.035 | 0.5 | 2.63-3.37 | 0.85-1.15 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  SA387-21L Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA387-21L | 205Mpa | 415-585Mpa | <=50MM | 18% |
|  | 205Mpa | 415-585Mpa | 50-200MM | -- |

6.  Normally SA387/SA387M SA387-21L plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA387-21L Delivery Time Or Lead Time: 20-35days

8.  SA387-21L Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA387-21L, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387-21L NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA387-21L,SA387/SA387M SA387-21L,SA387-21L Steel Plate,SA387-21L HIC,SA387-21L Nace

Tags: SA387-21L,SA387/SA387M SA387-21L,SA387-21L Steel Plate,SA387-21L steel factory, SA387-21L adopt standard, SA387-21L Heat treatment, SA387-21L Technical delivery condition, SA387-21L Chemical, SA387-21L Mechanical property, SA387-21L Price, SA387-21L CEV, SA387-21L Impact degree, SA387-21L impact energy, SA387-21L Supplier,SA387-21L Specification, SA387-21L properties, Material SA387-21L N, SA387-21L Material, SA387/SA387M, SA387-21L Steel, SA387-21L Yield, SA387-21L plate, SA387-21L HIC, SA387-21L NACE MR0175, SA387-21L ISO 15156, SA387-21L NACE MR0103, SA387-21L SSC