SA387-911,SA387-911 Steel Plate,SA387-911 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387-911 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. SA387-911,SA387/SA387M SA387-911,SA387-911 Steel Plate,SA387-911 HIC,SA387-911 Nace

Tags: SA387-911,SA387/SA387M SA387-911,SA387-911 Steel Plate,SA387-911 steel factory, SA387-911 adopt standard, SA387-911 Heat treatment, SA387-911 Technical delivery condition, SA387-911 Chemical, SA387-911 Mechanical property, SA387-911 Price, SA387-911 CEV, SA387-911 Impact degree, SA387-911 impact energy, SA387-911 Supplier,SA387-911 Specification, SA387-911 properties, Material SA387-911 N, SA387-911 Material, SA387/SA387M, SA387-911 Steel, SA387-911 Yield, SA387-911 plate, SA387-911 HIC, SA387-911 NACE MR0175, SA387-911 ISO 15156, SA387-911 NACE MR0103, SA387-911 SSC

Keyword: SA387-911,SA387-911 Steel Plate,SA387-911 Supplier

1.  SA387-911 Adopt standard: ASME SA387/SA387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  SA387-911 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA387-911: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA387-911 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA387-911 | 0.08-0.14 | 0.25-0.66 | 0.025 | 0.012 | 0.08-0.56 | 8.4-10.7 | 0.85-1.15 | 0.43 |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | 0.16-0.27 | 0.05-0.11 | 0.0002-0.007 | 0.035-0.095 | 0.05 | 0.85-1.15 |  |  |

5.  SA387-911 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA387-911 | 440Mpa | 620-840Mpa | <=50MM | 18% |
|  | 440Mpa | 620-840Mpa | 50-200MM | -- |

6.  Normally SA387/SA387M SA387-911 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA387-911 Delivery Time Or Lead Time: 20-35days

8.  SA387-911 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA387-911, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387-911 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA387-911,SA387/SA387M SA387-911,SA387-911 Steel Plate,SA387-911 HIC,SA387-911 Nace

Tags: SA387-911,SA387/SA387M SA387-911,SA387-911 Steel Plate,SA387-911 steel factory, SA387-911 adopt standard, SA387-911 Heat treatment, SA387-911 Technical delivery condition, SA387-911 Chemical, SA387-911 Mechanical property, SA387-911 Price, SA387-911 CEV, SA387-911 Impact degree, SA387-911 impact energy, SA387-911 Supplier,SA387-911 Specification, SA387-911 properties, Material SA387-911 N, SA387-911 Material, SA387/SA387M, SA387-911 Steel, SA387-911 Yield, SA387-911 plate, SA387-911 HIC, SA387-911 NACE MR0175, SA387-911 ISO 15156, SA387-911 NACE MR0103, SA387-911 SSC