SA387 GRADE 11,SA387 GRADE 11 Steel Plate,SA387 GRADE 11 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387 GRADE 11 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum Which is a large steel plate supplier mill at Gangsteel Group. SA387 GRADE 11,SA387/SA387M SA387 GRADE 11,SA387 GRADE 11 Steel Plate,SA387 GRADE 11 HIC,SA387 GRADE 11 Nace

Tags: SA387 GRADE 11,SA387/SA387M SA387 GRADE 11,SA387 GRADE 11 Steel Plate,SA387 GRADE 11 steel factory, SA387 GRADE 11 adopt standard, SA387 GRADE 11 Heat treatment, SA387 GRADE 11 Technical delivery condition, SA387 GRADE 11 Chemical, SA387 GRADE 11 Mechanical property, SA387 GRADE 11 Price, SA387 GRADE 11 CEV, SA387 GRADE 11 Impact degree, SA387 GRADE 11 impact energy, SA387 GRADE 11 Supplier,SA387 GRADE 11 Specification, SA387 GRADE 11 properties, Material SA387 GRADE 11 N, SA387 GRADE 11 Material, SA387/SA387M, SA387 GRADE 11 Steel, SA387 GRADE 11 Yield, SA387 GRADE 11 plate, SA387 GRADE 11 HIC, SA387 GRADE 11 NACE MR0175, SA387 GRADE 11 ISO 15156, SA387 GRADE 11 NACE MR0103, SA387 GRADE 11 SSC

Keyword: SA387 GRADE 11,SA387 GRADE 11 Steel Plate,SA387 GRADE 11 Supplier

1.  SA387 GRADE 11 Adopt standard: ASME SA387/SA387M Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Molybdenum

2.  SA387 GRADE 11 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA387 GRADE 11: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA387 GRADE 11 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Cr% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA387 GRADE 11 | 0.04-0.21 | 0.50-0.88 | 0.035 | 0.035 | 0.44-0.86 | 0.94-1.56 | 0.40-0.7 | -- |
|  | V% | Cb% | B% | N% | Al% | W% |  |  |
|  | -- | -- | -- | -- | -- | -- |  |  |

5.  SA387 GRADE 11 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA387 GRADE 11 | 240Mpa | 415-585Mpa | <=50MM | 22% |
|  | 240Mpa | 415-585Mpa | 50-200MM | 19% |

6.  Normally SA387/SA387M SA387 GRADE 11 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA387 GRADE 11 Delivery Time Or Lead Time: 20-35days

8.  SA387 GRADE 11 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA387 GRADE 11, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA387/SA387M SA387 GRADE 11 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA387 GRADE 11,SA387/SA387M SA387 GRADE 11,SA387 GRADE 11 Steel Plate,SA387 GRADE 11 HIC,SA387 GRADE 11 Nace

Tags: SA387 GRADE 11,SA387/SA387M SA387 GRADE 11,SA387 GRADE 11 Steel Plate,SA387 GRADE 11 steel factory, SA387 GRADE 11 adopt standard, SA387 GRADE 11 Heat treatment, SA387 GRADE 11 Technical delivery condition, SA387 GRADE 11 Chemical, SA387 GRADE 11 Mechanical property, SA387 GRADE 11 Price, SA387 GRADE 11 CEV, SA387 GRADE 11 Impact degree, SA387 GRADE 11 impact energy, SA387 GRADE 11 Supplier,SA387 GRADE 11 Specification, SA387 GRADE 11 properties, Material SA387 GRADE 11 N, SA387 GRADE 11 Material, SA387/SA387M, SA387 GRADE 11 Steel, SA387 GRADE 11 Yield, SA387 GRADE 11 plate, SA387 GRADE 11 HIC, SA387 GRADE 11 NACE MR0175, SA387 GRADE 11 ISO 15156, SA387 GRADE 11 NACE MR0103, SA387 GRADE 11 SSC