SA533 TYPE D,SA533 TYPE D Steel Plate,SA533 TYPE D Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA533/SA533M SA533 TYPE D NACE MR0175, MR0103 Boiler steel plate, Standard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel Which is a large steel plate supplier mill at Gangsteel Group. SA533 TYPE D,SA533/SA533M SA533 TYPE D,SA533 TYPE D Steel Plate,SA533 TYPE D HIC,SA533 TYPE D Nace

Tags: SA533 TYPE D,SA533/SA533M SA533 TYPE D,SA533 TYPE D Steel Plate,SA533 TYPE D steel factory, SA533 TYPE D adopt standard, SA533 TYPE D Heat treatment, SA533 TYPE D Technical delivery condition, SA533 TYPE D Chemical, SA533 TYPE D Mechanical property, SA533 TYPE D Price, SA533 TYPE D CEV, SA533 TYPE D Impact degree, SA533 TYPE D impact energy, SA533 TYPE D Supplier,SA533 TYPE D Specification, SA533 TYPE D properties, Material SA533 TYPE D N, SA533 TYPE D Material, SA533/SA533M, SA533 TYPE D Steel, SA533 TYPE D Yield, SA533 TYPE D plate, SA533 TYPE D HIC, SA533 TYPE D NACE MR0175, SA533 TYPE D ISO 15156, SA533 TYPE D NACE MR0103, SA533 TYPE D SSC

Keyword: SA533 TYPE D,SA533 TYPE D Steel Plate,SA533 TYPE D Supplier

1.  SA533 TYPE D Adopt standard: ASME SA533/SA533MStandard Specification for pressure Vessel Plates,Alloy Steel,Quenched and tempered,Manganese-Molybdenum and Manganese-Molybdenum-Nickel

2.  SA533 TYPE D Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA533 TYPE D: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA533 TYPE D Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Mo% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SA533 TYPE D | 0.25 | 1.07-1.82 | 0.035 | 0.035 | 0.13-0.45 | 0.41-0.84 | 0.17-0.43 |

5.  SA533 TYPE D Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA533 TYPE D | 570 Mpa | 690-860Mpa | <50MM | 16% |

6.  Normally SA533/SA533M SA533 TYPE D plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA533 TYPE D Delivery Time Or Lead Time: 20-35days

8.  SA533 TYPE D Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA533 TYPE D, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA533/SA533MSA533 TYPE D NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA533 TYPE D,SA533/SA533M SA533 TYPE D,SA533 TYPE D Steel Plate,SA533 TYPE D HIC,SA533 TYPE D Nace

Tags: SA533 TYPE D,SA533/SA533M SA533 TYPE D,SA533 TYPE D Steel Plate,SA533 TYPE D steel factory, SA533 TYPE D adopt standard, SA533 TYPE D Heat treatment, SA533 TYPE D Technical delivery condition, SA533 TYPE D Chemical, SA533 TYPE D Mechanical property, SA533 TYPE D Price, SA533 TYPE D CEV, SA533 TYPE D Impact degree, SA533 TYPE D impact energy, SA533 TYPE D Supplier,SA533 TYPE D Specification, SA533 TYPE D properties, Material SA533 TYPE D N, SA533 TYPE D Material, SA533/SA533M, SA533 TYPE D Steel, SA533 TYPE D Yield, SA533 TYPE D plate, SA533 TYPE D HIC, SA533 TYPE D NACE MR0175, SA533 TYPE D ISO 15156, SA533 TYPE D NACE MR0103, SA533 TYPE D SSC