JIS G 3103 SB480,SB480 Steel Plate,SB480 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB480 NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SB480,JIS G 3103 SB480,SB480 Steel Plate,SB480 HIC,SB480 Nace

Tags: SB480,JIS G 3103 SB480,SB480 Steel Plate,SB480 steel factory, SB480 adopt standard, SB480 Heat treatment, SB480 Technical delivery condition, SB480 Chemical, SB480 Mechanical property, SB480 Price, SB480 CEV, SB480 Impact degree, SB480 impact energy, SB480 Supplier,SB480 Specification, SB480 properties, Material SB480 N, SB480 Material, JIS G 3103, SB480 Steel, SB480 Yield, SB480 plate, SB480 HIC, SB480 NACE MR0175, SB480 ISO 15156, SB480 NACE MR0103, SB480 SSC

Keyword: SB480,SB480 Steel Plate,SB480 Supplier

1.  SB480 Adopt standard: ASMT JIS G 3103 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SB480 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SB480: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SB480 Chemical composition % of the Product analysis of grade

| Grade | C %(<25mm) | C %(25-50mm) | C%(>50mm) | Si% | Mn% | P% |
| --- | --- | --- | --- | --- | --- | --- |
| SB480 | 0.31 | 0.33 | 0.31 | 0.15-0.4 | 1.2 | 0.03 |
|  | S% | Mo% |  |  |  |  |
|  | 0.03 | -- |  |  |  |  |

5.  SB480 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SB480 | 265Mpa(min) | 480-620Mpa | <25mm | 17% |
|  | 265Mpa(min) | 480-620Mpa | 25-50mm | 17% |
|  | 265Mpa(min) | 480-620Mpa | 50-100mm | 21% |
|  | 265Mpa(min) | 480-620Mpa | >100mm | 21% |

6.  Normally JIS G 3103 SB480 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SB480 Delivery Time Or Lead Time: 20-35days

8.  SB480 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SB480, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB480 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SB480,JIS G 3103 SB480,SB480 Steel Plate,SB480 HIC,SB480 Nace

Tags: SB480,JIS G 3103 SB480,SB480 Steel Plate,SB480 steel factory, SB480 adopt standard, SB480 Heat treatment, SB480 Technical delivery condition, SB480 Chemical, SB480 Mechanical property, SB480 Price, SB480 CEV, SB480 Impact degree, SB480 impact energy, SB480 Supplier,SB480 Specification, SB480 properties, Material SB480 N, SB480 Material, JIS G 3103, SB480 Steel, SB480 Yield, SB480 plate, SB480 HIC, SB480 NACE MR0175, SB480 ISO 15156, SB480 NACE MR0103, SB480 SSC