JIS G 3103 SB480M,SB480M Steel Plate,SB480M Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB480M NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SB480M,JIS G 3103 SB480M,SB480M Steel Plate,SB480M HIC,SB480M Nace

Tags: SB480M,JIS G 3103 SB480M,SB480M Steel Plate,SB480M steel factory, SB480M adopt standard, SB480M Heat treatment, SB480M Technical delivery condition, SB480M Chemical, SB480M Mechanical property, SB480M Price, SB480M CEV, SB480M Impact degree, SB480M impact energy, SB480M Supplier,SB480M Specification, SB480M properties, Material SB480M N, SB480M Material, JIS G 3103, SB480M Steel, SB480M Yield, SB480M plate, SB480M HIC, SB480M NACE MR0175, SB480M ISO 15156, SB480M NACE MR0103, SB480M SSC

Keyword: SB480M,SB480M Steel Plate,SB480M Supplier

1.  SB480M Adopt standard: ASMT JIS G 3103 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SB480M Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SB480M: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SB480M Chemical composition % of the Product analysis of grade

| Grade | C %(<25mm) | C %(25-50mm) | C%(50-100mm) | C%(>100mm) | Si% | Mn% |
| --- | --- | --- | --- | --- | --- | --- |
| SB480M | 0.2 | 0.23 | 0.25 | 0.27 | 0.15-0.4 | 0.9 |
|  | P% | S% | Mo% |  |  |  |
|  | 0.03 | 0.03 | 0.45-0.6 |  |  |  |

5.  SB480M Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SB480M | 275Mpa(min) | 480-620Mpa | <25mm | 17% |
|  | 275Mpa(min) | 480-620Mpa | 25-100mm | 17% |
|  | 275Mpa(min) | 480-620Mpa | >100mm | 21% |

6.  Normally JIS G 3103 SB480M plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SB480M Delivery Time Or Lead Time: 20-35days

8.  SB480M Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SB480M, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G 3103 SB480M NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SB480M,JIS G 3103 SB480M,SB480M Steel Plate,SB480M HIC,SB480M Nace

Tags: SB480M,JIS G 3103 SB480M,SB480M Steel Plate,SB480M steel factory, SB480M adopt standard, SB480M Heat treatment, SB480M Technical delivery condition, SB480M Chemical, SB480M Mechanical property, SB480M Price, SB480M CEV, SB480M Impact degree, SB480M impact energy, SB480M Supplier,SB480M Specification, SB480M properties, Material SB480M N, SB480M Material, JIS G 3103, SB480M Steel, SB480M Yield, SB480M plate, SB480M HIC, SB480M NACE MR0175, SB480M ISO 15156, SB480M NACE MR0103, SB480M SSC