JIS G3115 SPV490,SPV490 Steel Plate,SPV490 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G3115 SPV490 NACE MR0175, MR0103 Boiler steel plate, Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels Which is a large steel plate supplier mill at Gangsteel Group. SPV490,JIS G3115 SPV490,SPV490 Steel Plate,SPV490 HIC,SPV490 Nace

Tags: SPV490,JIS G3115 SPV490,SPV490 Steel Plate,SPV490 steel factory, SPV490 adopt standard, SPV490 Heat treatment, SPV490 Technical delivery condition, SPV490 Chemical, SPV490 Mechanical property, SPV490 Price, SPV490 CEV, SPV490 Impact degree, SPV490 impact energy, SPV490 Supplier,SPV490 Specification, SPV490 properties, Material SPV490 N, SPV490 Material, JIS G3115, SPV490 Steel, SPV490 Yield, SPV490 plate, SPV490 HIC, SPV490 NACE MR0175, SPV490 ISO 15156, SPV490 NACE MR0103, SPV490 SSC

Keyword: SPV490,SPV490 Steel Plate,SPV490 Supplier

1.  SPV490 Adopt standard: ASMT JIS G3115 Carbon steel and molybdenum alloy steel plates for boilers and pressure vessels

2.  SPV490 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SPV490: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SPV490 Chemical composition % of the Product analysis of grade

| Grade | C % | Si% | Mn% | P% | S% |  |
| --- | --- | --- | --- | --- | --- | --- |
| SPV490 | 0.18 | 0.75 | 1.6 | 0.03 | 0.03 |  |

5.  SPV490 Mechanical Property

| Grade | Thicknesss | Min Yield | Tensile | Elongation |
| --- | --- | --- | --- | --- |
|  |  |  |  | Thicknesss |  |
| SPV490 | 6-50mm | 490Mpa(min) | 610-740Mpa | <=16mm | 18% |
|  | 50-100mm | 470Mpa(min) | 610-740Mpa | >16mm | 25% |
|  | 100-200mm | 450Mpa(min) | 610-740Mpa | >40mm | 19% |

6.  Normally JIS G3115 SPV490 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SPV490 Delivery Time Or Lead Time: 20-35days

8.  SPV490 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SPV490, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting JIS G3115 SPV490 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SPV490,JIS G3115 SPV490,SPV490 Steel Plate,SPV490 HIC,SPV490 Nace

Tags: SPV490,JIS G3115 SPV490,SPV490 Steel Plate,SPV490 steel factory, SPV490 adopt standard, SPV490 Heat treatment, SPV490 Technical delivery condition, SPV490 Chemical, SPV490 Mechanical property, SPV490 Price, SPV490 CEV, SPV490 Impact degree, SPV490 impact energy, SPV490 Supplier,SPV490 Specification, SPV490 properties, Material SPV490 N, SPV490 Material, JIS G3115, SPV490 Steel, SPV490 Yield, SPV490 plate, SPV490 HIC, SPV490 NACE MR0175, SPV490 ISO 15156, SPV490 NACE MR0103, SPV490 SSC