SA710-B,SA710-B Steel Plate,SA710-B Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710M SA710-B NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. SA710-B,SA710/SA710M SA710-B,SA710-B Steel Plate,SA710-B HIC,SA710-B Nace

Tags: SA710-B,SA710/SA710M SA710-B,SA710-B Steel Plate,SA710-B steel factory, SA710-B adopt standard, SA710-B Heat treatment, SA710-B Technical delivery condition, SA710-B Chemical, SA710-B Mechanical property, SA710-B Price, SA710-B CEV, SA710-B Impact degree, SA710-B impact energy, SA710-B Supplier,SA710-B Specification, SA710-B properties, Material SA710-B N, SA710-B Material, SA710/SA710M, SA710-B Steel, SA710-B Yield, SA710-B plate, SA710-B HIC, SA710-B NACE MR0175, SA710-B ISO 15156, SA710-B NACE MR0103, SA710-B SSC

Keyword: SA710-B,SA710-B Steel Plate,SA710-B Supplier

1.  SA710-B Adopt standard: ASME SA710/SA710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  SA710-B Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA710-B: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA710-B Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| SA710-B | 0.03-0.09 | 0.45-1.3 | 0.025 | 0.025 | 0.3-0.5 | 0.8-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.25 | 1.25-1.5 | 0.05-0.06 | 0.01-0.03 | 0.3 |  |

5.  SA710-B Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA710-B | 485Mpa | 550Mpa | <6.5mm | 20% |
|  | 485Mpa | 550Mpa | 6.5-8mm | 20% |
|  | 485Mpa | 550Mpa | 8-10mm | 20% |
|  | 485Mpa | 550Mpa | 10-12.5mm | 20% |
|  | 485Mpa | 550Mpa | 12.5-20mm | 20% |
|  | 485Mpa | 550Mpa | 20-25mm | 20% |
|  | --- | --- | 25-30mm | 20% |
|  | --- | --- | 30-50mm | 20% |
|  | --- | --- | 50-100mm | -- |
|  | --- | --- | >100mm | -- |

6.  Normally SA710/SA710M SA710-B plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA710-B Delivery Time Or Lead Time: 20-35days

8.  SA710-B Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA710-B, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710MSA710-B NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA710-B,SA710/SA710M SA710-B,SA710-B Steel Plate,SA710-B HIC,SA710-B Nace

Tags: SA710-B,SA710/SA710M SA710-B,SA710-B Steel Plate,SA710-B steel factory, SA710-B adopt standard, SA710-B Heat treatment, SA710-B Technical delivery condition, SA710-B Chemical, SA710-B Mechanical property, SA710-B Price, SA710-B CEV, SA710-B Impact degree, SA710-B impact energy, SA710-B Supplier,SA710-B Specification, SA710-B properties, Material SA710-B N, SA710-B Material, SA710/SA710M, SA710-B Steel, SA710-B Yield, SA710-B plate, SA710-B HIC, SA710-B NACE MR0175, SA710-B ISO 15156, SA710-B NACE MR0103, SA710-B SSC