SA710GRA,SA710GRA Steel Plate,SA710GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710M SA710GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. SA710GRA,SA710/SA710M SA710GRA,SA710GRA Steel Plate,SA710GRA HIC,SA710GRA Nace

Tags: SA710GRA,SA710/SA710M SA710GRA,SA710GRA Steel Plate,SA710GRA steel factory, SA710GRA adopt standard, SA710GRA Heat treatment, SA710GRA Technical delivery condition, SA710GRA Chemical, SA710GRA Mechanical property, SA710GRA Price, SA710GRA CEV, SA710GRA Impact degree, SA710GRA impact energy, SA710GRA Supplier,SA710GRA Specification, SA710GRA properties, Material SA710GRA N, SA710GRA Material, SA710/SA710M, SA710GRA Steel, SA710GRA Yield, SA710GRA plate, SA710GRA HIC, SA710GRA NACE MR0175, SA710GRA ISO 15156, SA710GRA NACE MR0103, SA710GRA SSC

Keyword: SA710GRA,SA710GRA Steel Plate,SA710GRA Supplier

1.  SA710GRA Adopt standard: ASME SA710/SA710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  SA710GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA710GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA710GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| SA710GRA | 0.07 | 0.40-0.70 | 0.025 | 0.025 | 0.4 | 0.7-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.15-0.25 | 1.0-1.3 | 0.02 | -- | 0.6-0.9 |  |

5.  SA710GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA710GRA | 550Mpa | 585Mpa | <6.5mm | 20% |
|  | 585Mpa | 585Mpa | 6.5-8mm | 20% |
|  | 550Mpa | 585Mpa | 8-10mm | 20% |
|  | 550Mpa | 585Mpa | 10-12.5mm | 20% |
|  | 550Mpa | 585Mpa | 12.5-20mm | 20% |
|  | 550Mpa | 585Mpa | 20-25mm | 20% |
|  | 550Mpa | 585Mpa | 25-30mm | 20% |
|  | 515Mpa | 585Mpa | 30-50mm | 20% |
|  | 450Mpa | 515Mpa | 50-100mm | -- |
|  | 415Mpa | 485Mpa | >100mm | -- |

6.  Normally SA710/SA710M SA710GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA710GRA Delivery Time Or Lead Time: 20-35days

8.  SA710GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA710GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710MSA710GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA710GRA,SA710/SA710M SA710GRA,SA710GRA Steel Plate,SA710GRA HIC,SA710GRA Nace

Tags: SA710GRA,SA710/SA710M SA710GRA,SA710GRA Steel Plate,SA710GRA steel factory, SA710GRA adopt standard, SA710GRA Heat treatment, SA710GRA Technical delivery condition, SA710GRA Chemical, SA710GRA Mechanical property, SA710GRA Price, SA710GRA CEV, SA710GRA Impact degree, SA710GRA impact energy, SA710GRA Supplier,SA710GRA Specification, SA710GRA properties, Material SA710GRA N, SA710GRA Material, SA710/SA710M, SA710GRA Steel, SA710GRA Yield, SA710GRA plate, SA710GRA HIC, SA710GRA NACE MR0175, SA710GRA ISO 15156, SA710GRA NACE MR0103, SA710GRA SSC