SA710GRB,SA710GRB Steel Plate,SA710GRB Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710M SA710GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates, Which is a large steel plate supplier mill at Gangsteel Group. SA710GRB,SA710/SA710M SA710GRB,SA710GRB Steel Plate,SA710GRB HIC,SA710GRB Nace

Tags: SA710GRB,SA710/SA710M SA710GRB,SA710GRB Steel Plate,SA710GRB steel factory, SA710GRB adopt standard, SA710GRB Heat treatment, SA710GRB Technical delivery condition, SA710GRB Chemical, SA710GRB Mechanical property, SA710GRB Price, SA710GRB CEV, SA710GRB Impact degree, SA710GRB impact energy, SA710GRB Supplier,SA710GRB Specification, SA710GRB properties, Material SA710GRB N, SA710GRB Material, SA710/SA710M, SA710GRB Steel, SA710GRB Yield, SA710GRB plate, SA710GRB HIC, SA710GRB NACE MR0175, SA710GRB ISO 15156, SA710GRB NACE MR0103, SA710GRB SSC

Keyword: SA710GRB,SA710GRB Steel Plate,SA710GRB Supplier

1.  SA710GRB Adopt standard: ASME SA710/SA710M Standard Specification for Precipitation-Strengthened Low-Carbon Nickel-copper-Chromium-Molybdenum-Columbium Alloy Structural Steel Plates.

2.  SA710GRB Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA710GRB: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA710GRB Chemical composition % of the Product analysis of grade

| Grade | C % | Mn % | P% | S% | Si% | Ni% |
| --- | --- | --- | --- | --- | --- | --- |
| SA710GRB | 0.03-0.09 | 0.45-1.3 | 0.025 | 0.025 | 0.3-0.5 | 0.8-1.0 |
|  | Mo% | Cu% | Cb% | Ti% | Cr% |  |
|  | 0.25 | 1.25-1.5 | 0.05-0.06 | 0.01-0.03 | 0.3 |  |

5.  SA710GRB Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA710GRB | 485Mpa | 550Mpa | <6.5mm | 20% |
|  | 485Mpa | 550Mpa | 6.5-8mm | 20% |
|  | 485Mpa | 550Mpa | 8-10mm | 20% |
|  | 485Mpa | 550Mpa | 10-12.5mm | 20% |
|  | 485Mpa | 550Mpa | 12.5-20mm | 20% |
|  | 485Mpa | 550Mpa | 20-25mm | 20% |
|  | --- | --- | 25-30mm | 20% |
|  | --- | --- | 30-50mm | 20% |
|  | --- | --- | 50-100mm | -- |
|  | --- | --- | >100mm | -- |

6.  Normally SA710/SA710M SA710GRB plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA710GRB Delivery Time Or Lead Time: 20-35days

8.  SA710GRB Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA710GRB, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA710/SA710MSA710GRB NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA710GRB,SA710/SA710M SA710GRB,SA710GRB Steel Plate,SA710GRB HIC,SA710GRB Nace

Tags: SA710GRB,SA710/SA710M SA710GRB,SA710GRB Steel Plate,SA710GRB steel factory, SA710GRB adopt standard, SA710GRB Heat treatment, SA710GRB Technical delivery condition, SA710GRB Chemical, SA710GRB Mechanical property, SA710GRB Price, SA710GRB CEV, SA710GRB Impact degree, SA710GRB impact energy, SA710GRB Supplier,SA710GRB Specification, SA710GRB properties, Material SA710GRB N, SA710GRB Material, SA710/SA710M, SA710GRB Steel, SA710GRB Yield, SA710GRB plate, SA710GRB HIC, SA710GRB NACE MR0175, SA710GRB ISO 15156, SA710GRB NACE MR0103, SA710GRB SSC