SA738 GRADE A,SA738 GRADE A Steel Plate,SA738 GRADE A Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738 GRADE A NACE MR0175, MR0103 Boiler steel plate, Specification for pressure plates,heat-treated,carbon-manganese-silicon steel ,for moderate and lower temperature service. Which is a large steel plate supplier mill at Gangsteel Group. SA738 GRADE A,SA-738/SA-738M SA738 GRADE A,SA738 GRADE A Steel Plate,SA738 GRADE A HIC,SA738 GRADE A Nace

Tags: SA738 GRADE A,SA-738/SA-738M SA738 GRADE A,SA738 GRADE A Steel Plate,SA738 GRADE A steel factory, SA738 GRADE A adopt standard, SA738 GRADE A Heat treatment, SA738 GRADE A Technical delivery condition, SA738 GRADE A Chemical, SA738 GRADE A Mechanical property, SA738 GRADE A Price, SA738 GRADE A CEV, SA738 GRADE A Impact degree, SA738 GRADE A impact energy, SA738 GRADE A Supplier,SA738 GRADE A Specification, SA738 GRADE A properties, Material SA738 GRADE A N, SA738 GRADE A Material, SA-738/SA-738M, SA738 GRADE A Steel, SA738 GRADE A Yield, SA738 GRADE A plate, SA738 GRADE A HIC, SA738 GRADE A NACE MR0175, SA738 GRADE A ISO 15156, SA738 GRADE A NACE MR0103, SA738 GRADE A SSC

Keyword: SA738 GRADE A,SA738 GRADE A Steel Plate,SA738 GRADE A Supplier

1.  SA738 GRADE A Adopt standard: ASME SA-738/SA-738M Specification for pressure plates,heat-treated,carbon-manganese-silicon steel.

2.  SA738 GRADE A Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA738 GRADE A: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA738 GRADE A Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<65mm) | Mn %(>65mm) | P% | S% | Si% | Cu% | Ni% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA738 GRADE A | 0.24 | 1.62 | 1.72 | 0.035 | 0.035 | 0.13-0.55 | 0.38 | 0.53 |
|  | Cr% | Mo%(40mm) | Mo%(<40mm) | V% | Cb% | Cb plus V |  |  |
|  | 0.29 | 0.08 | 0.08 | 0.08 | 0.05 | 0.10 |  |  |

5.  SA738 GRADE A Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA738 GRADE A | 310 Mpa | 515-655Mpa | <65MM | 20% |
|  | 310 Mpa | 515-655Mpa | 65-100MM | 20% |
|  | 310 Mpa | 515-655Mpa | >100MM | 20% |

6.  Normally SA-738/SA-738M SA738 GRADE A plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA738 GRADE A Delivery Time Or Lead Time: 20-35days

8.  SA738 GRADE A Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA738 GRADE A, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-738/SA-738M SA738 GRADE A NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA738 GRADE A,SA-738/SA-738M SA738 GRADE A,SA738 GRADE A Steel Plate,SA738 GRADE A HIC,SA738 GRADE A Nace

Tags: SA738 GRADE A,SA-738/SA-738M SA738 GRADE A,SA738 GRADE A Steel Plate,SA738 GRADE A steel factory, SA738 GRADE A adopt standard, SA738 GRADE A Heat treatment, SA738 GRADE A Technical delivery condition, SA738 GRADE A Chemical, SA738 GRADE A Mechanical property, SA738 GRADE A Price, SA738 GRADE A CEV, SA738 GRADE A Impact degree, SA738 GRADE A impact energy, SA738 GRADE A Supplier,SA738 GRADE A Specification, SA738 GRADE A properties, Material SA738 GRADE A N, SA738 GRADE A Material, SA-738/SA-738M, SA738 GRADE A Steel, SA738 GRADE A Yield, SA738 GRADE A plate, SA738 GRADE A HIC, SA738 GRADE A NACE MR0175, SA738 GRADE A ISO 15156, SA738 GRADE A NACE MR0103, SA738 GRADE A SSC