SA841CL3,SA841CL3 Steel Plate,SA841CL3 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA841CL3 NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. SA841CL3,SA-841/SA-841M SA841CL3,SA841CL3 Steel Plate,SA841CL3 HIC,SA841CL3 Nace

Tags: SA841CL3,SA-841/SA-841M SA841CL3,SA841CL3 Steel Plate,SA841CL3 steel factory, SA841CL3 adopt standard, SA841CL3 Heat treatment, SA841CL3 Technical delivery condition, SA841CL3 Chemical, SA841CL3 Mechanical property, SA841CL3 Price, SA841CL3 CEV, SA841CL3 Impact degree, SA841CL3 impact energy, SA841CL3 Supplier,SA841CL3 Specification, SA841CL3 properties, Material SA841CL3 N, SA841CL3 Material, SA-841/SA-841M, SA841CL3 Steel, SA841CL3 Yield, SA841CL3 plate, SA841CL3 HIC, SA841CL3 NACE MR0175, SA841CL3 ISO 15156, SA841CL3 NACE MR0103, SA841CL3 SSC

Keyword: SA841CL3,SA841CL3 Steel Plate,SA841CL3 Supplier

1.  SA841CL3 Adopt standard: ASME SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  SA841CL3 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA841CL3: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA841CL3 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA841CL3 | 0.09 | 1.0-2.0 | 0.01 | 0.005 | 0.05-0.25 | 0.5 | 1.0-5.0 | 0.3 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.4 | 0.05 | 0.02 | -- | 0.006-0.03 | 0.0005-0.002 |  |  |

5.  SA841CL3 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA841CL3 | 690 Mpa | 1000-1170Mpa | <40MM | 13% |
|  | -- | -- | 40-65MM | -- |
|  | -- | -- | >65MM | -- |

6.  Normally SA-841/SA-841M SA841CL3 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA841CL3 Delivery Time Or Lead Time: 20-35days

8.  SA841CL3 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA841CL3, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA841CL3 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA841CL3,SA-841/SA-841M SA841CL3,SA841CL3 Steel Plate,SA841CL3 HIC,SA841CL3 Nace

Tags: SA841CL3,SA-841/SA-841M SA841CL3,SA841CL3 Steel Plate,SA841CL3 steel factory, SA841CL3 adopt standard, SA841CL3 Heat treatment, SA841CL3 Technical delivery condition, SA841CL3 Chemical, SA841CL3 Mechanical property, SA841CL3 Price, SA841CL3 CEV, SA841CL3 Impact degree, SA841CL3 impact energy, SA841CL3 Supplier,SA841CL3 Specification, SA841CL3 properties, Material SA841CL3 N, SA841CL3 Material, SA-841/SA-841M, SA841CL3 Steel, SA841CL3 Yield, SA841CL3 plate, SA841CL3 HIC, SA841CL3 NACE MR0175, SA841CL3 ISO 15156, SA841CL3 NACE MR0103, SA841CL3 SSC