SA841GRA,SA841GRA Steel Plate,SA841GRA Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA841GRA NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. SA841GRA,SA-841/SA-841M SA841GRA,SA841GRA Steel Plate,SA841GRA HIC,SA841GRA Nace

Tags: SA841GRA,SA-841/SA-841M SA841GRA,SA841GRA Steel Plate,SA841GRA steel factory, SA841GRA adopt standard, SA841GRA Heat treatment, SA841GRA Technical delivery condition, SA841GRA Chemical, SA841GRA Mechanical property, SA841GRA Price, SA841GRA CEV, SA841GRA Impact degree, SA841GRA impact energy, SA841GRA Supplier,SA841GRA Specification, SA841GRA properties, Material SA841GRA N, SA841GRA Material, SA-841/SA-841M, SA841GRA Steel, SA841GRA Yield, SA841GRA plate, SA841GRA HIC, SA841GRA NACE MR0175, SA841GRA ISO 15156, SA841GRA NACE MR0103, SA841GRA SSC

Keyword: SA841GRA,SA841GRA Steel Plate,SA841GRA Supplier

1.  SA841GRA Adopt standard: ASME SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  SA841GRA Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA841GRA: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA841GRA Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA841GRA | 0.2 | 0.7-1.35 | 0.03 | 0.03 | 0.15-0.5 | 0.35 | 0.25 | 0.25 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.08 | 0.03 | 0.06 | 1.0-1.6 | -- | -- |  |  |

5.  SA841GRA Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA841GRA | 345 Mpa | 480-620Mpa | <40MM | 22% |
|  | 345 Mpa | 480-620Mpa | 40-65MM | 22% |
|  | 310 Mpa | 450-585Mpa | >65MM | 22% |

6.  Normally SA-841/SA-841M SA841GRA plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA841GRA Delivery Time Or Lead Time: 20-35days

8.  SA841GRA Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA841GRA, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA841GRA NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA841GRA,SA-841/SA-841M SA841GRA,SA841GRA Steel Plate,SA841GRA HIC,SA841GRA Nace

Tags: SA841GRA,SA-841/SA-841M SA841GRA,SA841GRA Steel Plate,SA841GRA steel factory, SA841GRA adopt standard, SA841GRA Heat treatment, SA841GRA Technical delivery condition, SA841GRA Chemical, SA841GRA Mechanical property, SA841GRA Price, SA841GRA CEV, SA841GRA Impact degree, SA841GRA impact energy, SA841GRA Supplier,SA841GRA Specification, SA841GRA properties, Material SA841GRA N, SA841GRA Material, SA-841/SA-841M, SA841GRA Steel, SA841GRA Yield, SA841GRA plate, SA841GRA HIC, SA841GRA NACE MR0175, SA841GRA ISO 15156, SA841GRA NACE MR0103, SA841GRA SSC