SA841GRD,SA841GRD Steel Plate,SA841GRD Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA841GRD NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. SA841GRD,SA-841/SA-841M SA841GRD,SA841GRD Steel Plate,SA841GRD HIC,SA841GRD Nace

Tags: SA841GRD,SA-841/SA-841M SA841GRD,SA841GRD Steel Plate,SA841GRD steel factory, SA841GRD adopt standard, SA841GRD Heat treatment, SA841GRD Technical delivery condition, SA841GRD Chemical, SA841GRD Mechanical property, SA841GRD Price, SA841GRD CEV, SA841GRD Impact degree, SA841GRD impact energy, SA841GRD Supplier,SA841GRD Specification, SA841GRD properties, Material SA841GRD N, SA841GRD Material, SA-841/SA-841M, SA841GRD Steel, SA841GRD Yield, SA841GRD plate, SA841GRD HIC, SA841GRD NACE MR0175, SA841GRD ISO 15156, SA841GRD NACE MR0103, SA841GRD SSC

Keyword: SA841GRD,SA841GRD Steel Plate,SA841GRD Supplier

1.  SA841GRD Adopt standard: ASME SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  SA841GRD Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA841GRD: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA841GRD Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA841GRD | 0.09 | 1.0-2.0 | 0.01 | 0.005 | 0.05-0.25 | 0.5 | 1.0-5.0 | 0.3 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.4 | 0.05 | 0.02 | -- | 0.006-0.03 | 0.0005-0.002 |  |  |

5.  SA841GRD Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA841GRD | 690 Mpa | 1000-1170Mpa | <40MM | 13% |
|  | -- | -- | 40-65MM | -- |
|  | -- | -- | >65MM | -- |

6.  Normally SA-841/SA-841M SA841GRD plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

7.  SA841GRD Delivery Time Or Lead Time: 20-35days

8.  SA841GRD Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

9.  If you have any requirement in steel plate for SA841GRD, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA841GRD NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA841GRD,SA-841/SA-841M SA841GRD,SA841GRD Steel Plate,SA841GRD HIC,SA841GRD Nace

Tags: SA841GRD,SA-841/SA-841M SA841GRD,SA841GRD Steel Plate,SA841GRD steel factory, SA841GRD adopt standard, SA841GRD Heat treatment, SA841GRD Technical delivery condition, SA841GRD Chemical, SA841GRD Mechanical property, SA841GRD Price, SA841GRD CEV, SA841GRD Impact degree, SA841GRD impact energy, SA841GRD Supplier,SA841GRD Specification, SA841GRD properties, Material SA841GRD N, SA841GRD Material, SA-841/SA-841M, SA841GRD Steel, SA841GRD Yield, SA841GRD plate, SA841GRD HIC, SA841GRD NACE MR0175, SA841GRD ISO 15156, SA841GRD NACE MR0103, SA841GRD SSC