SA84CL2,SA84CL2 Steel Plate,SA84CL2 Supplier

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA84CL2 NACE MR0175, MR0103 Boiler steel plate, Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP) Which is a large steel plate supplier mill at Gangsteel Group. SA84CL2,SA-841/SA-841M SA84CL2,SA84CL2 Steel Plate,SA84CL2 HIC,SA84CL2 Nace

Tags: SA84CL2,SA-841/SA-841M SA84CL2,SA84CL2 Steel Plate,SA84CL2 steel factory, SA84CL2 adopt standard, SA84CL2 Heat treatment, SA84CL2 Technical delivery condition, SA84CL2 Chemical, SA84CL2 Mechanical property, SA84CL2 Price, SA84CL2 CEV, SA84CL2 Impact degree, SA84CL2 impact energy, SA84CL2 Supplier,SA84CL2 Specification, SA84CL2 properties, Material SA84CL2 N, SA84CL2 Material, SA-841/SA-841M, SA84CL2 Steel, SA84CL2 Yield, SA84CL2 plate, SA84CL2 HIC, SA84CL2 NACE MR0175, SA84CL2 ISO 15156, SA84CL2 NACE MR0103, SA84CL2 SSC

Keyword: SA84CL2,SA84CL2 Steel Plate,SA84CL2 Supplier

1.  SA84CL2 Adopt standard: ASME SA-841/SA-841M Specification for Steel plates for pressure vessels,produced by the thermo mechanical control process(TMCP)

2.  SA84CL2 Specification:  Thickness: 5mm to 200mm; Width: 1500mm to 3500mm: Length: 3000mm to 27000mm

3.  Third Party Inspection for SA84CL2: ABS, DNV, BV, GL, CCS, LR, RINA, KR, NK, CE, SGS, IKE, IEI or other quality department.

4.  SA84CL2 Chemical composition % of the Product analysis of grade

| Grade | C % | Mn %(<40mm) | P% | S% | Si% | Cu% | Ni% | Cr% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SA84CL2 | 0.15 | 0.7-1.35 | 0.03 | 0.025 | 0.15-0.5 | 0.35 | 0.6 | 0.25 |
|  | Mo% | Cb% | V% | Mn %(>40mm) | Ti% | B% |  |  |
|  | 0.3 | 0.03 | 0.06 | 1.0-1.6 | -- | -- |  |  |

4.  SA84CL2 Mechanical Property

| Grade | Min Yield | Tensile | Thicknesss | Elongation |
| --- | --- | --- | --- | --- |
| SA84CL2 | 415 Mpa | 550-690Mpa | <40MM | 22% |
|  | 415 Mpa | 550-690Mpa | 40-65MM | 22% |
|  | 380 Mpa | 515-655Mpa | >65MM | 22% |

5.  Normally SA-841/SA-841M SA84CL2 plates are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both.

6.  SA84CL2 Delivery Time Or Lead Time: 20-35days

7.  SA84CL2 Extra Service: Pretreatment (Shot Blasting, Sand Blast, Painting and Galvanized), Cutting Parts, Sample Service, Third Party inspection, UT Test and Size inspection.

8.  If you have any requirement in steel plate for SA84CL2, whether the new plate or stock list of material, please feel free to contact us by email of calling.

If you had any question at our plate or service. Please contact our after service department to get faster reply

.

Gangsteel Group Company Principle

More Cheaper Price,

More Faster Delivery,

The Best Company Prestige,

The Best After sales service,

The One step Steel material Solution

The Best Professional quality control system

Supplementary Requirements

S2. Product Analysis,       S8: Ultrasonic Examination

S3: Simulated pos-weld heat treatment of mechanical

S15: Reduction of area measurement and test coupons

S18: Maximum Tensile strength

S6: Drop weight test

S30：Charpy V notch impact test for structural shapes

Welcome to Gangsteel Group and any requirement in steel material, please feel free to contact us.

Gangsteel Bolier Plate Factory are specialized in producing and exporting SA-841/SA-841M SA84CL2 NACE MR0175, MR0103 Boiler steel plate, Standard Specification for Pressure Vessel Plates, Alloy Steel, Chromium-Manganese-Silicon Which is a large steel plate supplier mill at Gangsteel Group. SA84CL2,SA-841/SA-841M SA84CL2,SA84CL2 Steel Plate,SA84CL2 HIC,SA84CL2 Nace

Tags: SA84CL2,SA-841/SA-841M SA84CL2,SA84CL2 Steel Plate,SA84CL2 steel factory, SA84CL2 adopt standard, SA84CL2 Heat treatment, SA84CL2 Technical delivery condition, SA84CL2 Chemical, SA84CL2 Mechanical property, SA84CL2 Price, SA84CL2 CEV, SA84CL2 Impact degree, SA84CL2 impact energy, SA84CL2 Supplier,SA84CL2 Specification, SA84CL2 properties, Material SA84CL2 N, SA84CL2 Material, SA-841/SA-841M, SA84CL2 Steel, SA84CL2 Yield, SA84CL2 plate, SA84CL2 HIC, SA84CL2 NACE MR0175, SA84CL2 ISO 15156, SA84CL2 NACE MR0103, SA84CL2 SSC