S355J0W Weathering Steel

1.Weather Resistant Steel

Corten Steel | Corten A | Corten B | S355J0WP | S355J0W | S355J2W

2.S355J0W – an equivalent to Corten B and used in heavy load bearing applications. Like S355J0WP, S355J0W is a weathering steel and is an equivalent to Corten B.

3.As the material rusts when exposed to atmospheric elements, the material builds its own protective layer which prevents the steel from further oxidation. Therefore S355J0W, like all weathering steels, offers excellent, cost effective protection against atmospheric conditions without the need for painting or external treatment.

4.S355J0WP tends to be used for structures which use thinner materials.

Grades & Equivalents

| EN 10025-5:2004 | Corten |
| --- | --- |
| S355J0W | Corten B |

5.Chemical Composition

| Grade | C | Si | Mn | P | S | N | Addition of nitrogen binding elements | Cr | Cu |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S355J0W | 0.16 | 0.50 | 0.50/1.50 | 0.035 | 0.035 | 0.009 | – | 0.40/0.80 | 0.25/0.55 |

Maximum values unless otherwise stated

6.Mechanical Properties

| Grade | Min. Yield Strength Reh MPa | Tensile Strength Rm MPa |
| --- | --- | --- |
|  | Nominal Thickness (mm) | Nominal Thickness (mm) |
|  | ≤16 | >16 ≤40 | >40 ≤63 | >63 ≤80 | >80 ≤100 | >100 ≤150 | >3 | >3 ≤100 | >100 ≤150 |
| S355J0W | 355 | 345 | 335 | 325 | 315 | 295 | 510/680 | 470/630 | 450/600 |

(Please note: the technical information above is for guidance only – for exact specifications please check with our Sales Team)

7.Buy S355J0W from one of Europe' major steel stockholders – Please contact us today.