A516 Grade 70 Steel Plate, A516 Gr.70 Supplier

1. A516 steel plate, also known as PVQ516 steel plate, is carbon steel with specifications for pressure vessel plates and moderate or lower temperature service. A516 steel plate is intended primarily for service in welded pressure vessels where improved notch toughness is important. Plates 1.50” and under in thickness are normally supplied in the as-rolled condition. The plates may be ordered normalized or stress relieved, or both. Plates over 1.50” in thickness shall be normalized.

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| PVQ Pressure Vessel Steel Plate | | | | |
| all measurement in Inches | | Thickness | Width | Length |
| A516 | Grade 55 | 3/16" – 6" | 48" – 120" | 96" – 480" |
| Grade 60 | 3/16" – 6" | 48" – 120" | 96" – 480" |
| Grade 65 | 3/16" – 6" | 48" – 120" | 96" – 480" |
| Grade 70 | 3/16" – 6" | 48" – 120" | 96" – 480" |

2. If you have any other requirement for steel plate, please feel free to contact us.