DNV FH36 STEEL PLATE

Gangsteel is specialized in supplying DNV high strength steel plate in DNV Grade F36. For more information of Grade F36 steel plate, please check them in following:

| DNV FH36 high Strength Chemical Composition |
| --- |
| Grade | The Element Max (%) |
|  | C | Si | Mn | P | S | Al | N |
| DNV FH36 | 0.16 | 0.10-0.50 | 0.9-1.6 | 0.025 | 0.025 | 0.015-0.08 | 0.009 |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.05-0.10 | 0.02 | 0.35 | 0.20 | 0.80 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| DNV FH36 high general strength property |
| --- |
| Grade |  | Mechanical Property | Charpy V Impact Test |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| DNV FH36 | mm | Min Mpa | Mpa | Min % | -60 | J | J |
|  | t≤50 | 355 | 490-620 | 21% |  | 24 | 34 |
|  | 50＜t≤70 | 355 | 490-620 | 21% |  | 27 | 41 |
|  | 70＜t≤150 | 355 | 490-620 | 21% |  | 34 | 50 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of DNV FH36 |
| --- |
| ABS | GL | LR | BV | CCS | NK | KR | RINA |
| AB/F36 | GL-F36 | LR/F36 | BV/F36 | CCS/F36 | K F36 | R F36 | RI/F36 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.