LR/DH40 STEEL PLATE

Gangsteel is specialized in supplying LR high strength steel plate in LR Grade DH40. For more information of Grade DH40 steel plate, please check them in following:

| LR/DH40 high Strength Chemical Composition |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al | N |
| LR/DH40 | 0.18 | 0.05 | 0.9-1.6 | 0.035 | 0.035 | 0.015 |  |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.03-0.10 | 0.02 | 0.35 | 0.20 | 0.40 | 0.08 |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| LR/DH40 high strength property |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| LR/DH40 | mm | Min Mpa | Mpa | Min % | -20 | J | J |
|  | t≤50 | 390 | 510-650 | 20% |  | 26 | 39 |
|  | 50＜t≤70 | 390 | 510-650 | 20% |  | 31 | 46 |
|  | 70＜t≤100 | 390 | 510-650 | 20% |  | 37 | 55 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of LR/DH40 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | ABS | BV | CCS | NK | KR | RINA |
| NV D40 | GL-D40 | AB/DH40 | BV/DH40 | CCS/D40 | K D40 | R D40 | RI/D40 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.