LR/FH50 STEEL PLATE

Gangsteel is specialized in supplying LR extra strength steel plate in LR Grade FH50. For more information of Grade FH50 steel plate, please check them in following:

| LR/FH50 extra high Strength Chemical Composition |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al | N |
| LR/FH50 | 0.18 | 0.55 | 1.60 | 0.025 | 0.025 | 0.015 | 0.020 |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |
|  | 0.02-0.05 | 0.03-0.10 | 0.02 |  |  |  |  |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| LR/FH50 extra high strength property |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| LR/FH50 | mm | Min Mpa | Mpa | Min % | -60 | J | J |
|  | t≤50 | 500 | 610-770 | 18% |  | 33 | 50 |
|  | 50＜t≤70 | 500 | 610-770 | 18% |  | 33 | 50 |
|  | 70＜t≤100 | 500 | 610-770 | 18% |  | 33 | 50 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of LR/FH50 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | ABS | BV | CCS | NK | KR | RINA |
| NV F500 | GL-F500 | AB/FQ51 | BV/F500 | CCS/F500 | K F51 | R F51 | RI/F500 |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.