LR/B STEEL PLATE

Gangsteel is specialized in supplying LR general strength steel plate in LR Grade B. For more information of Grade B steel plate, please check them in following:

| LR/B general Strength Chemical Composition |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade | The Element Max (%) |  |  |  |  |  |  |
|  | C | Si | Mn | P | S | Al | N |
| LR/B | 0.21 | 0.35 | 0.80 | 0.035 | 0.035 |  |  |
|  | Nb | V | Ti | Cu | Cr | Ni | Mo |

Crack Sensitivity:  Pcm = (C+Si/30+Mn/20+Cu/20+Ni/60+Cr/20+Mo/15+V/10+5B)%
Carbon Equivalent:  Ceq = 【C+Mn/6+(Cr+Mo+V)/5+(Ni+Cu)/15】%

| LR/B general strength property |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Grade |  | Mechanical Property |  |  | Charpy V Impact Test |  |  |
|  | Thickness | Yield | Tensile | Elongation | Degree | Energy 1 | Energy 2 |
| LR/B | mm | Min Mpa | Mpa | Min % | 0 | J | J |
|  | t≤50 | 235 | 400-520 | 22% |  | 20 | 27 |
|  | 50＜t≤70 | 235 | 400-520 | 22% |  | 24 | 34 |
|  | 70＜t≤100 | 235 | 400-520 | 22% |  | 27 | 41 |
| Note: Energy 1 is transverse impact test, Energy 2 is longitudinal |  |  |  |  |  |  |  |

Boiler steel plates | Alloy steel plates | High strength plate| Carbon steel plate | Stainless steel plate

| Equivalent steel grade of LR/B |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DNV | GL | ABS | BV | CCS | NK | KR | RINA |
| NV B | GL-B | AB/B | BV/B | CCS/B | K B | R B | RI/B |

If you need more stock steel plates in shipbuilding steel plate, please click warehouse sizes.